## Slide 1: Lyophilization Process Development for Biopharmaceuticals Applications for eis PAT
Friday 23rd October 2020
Prof. Geoff Smith
eis
Electrical
Impedance
Spectroscopy
PAT
Process
Analytical
Technology
Notes: Hello and welcome to my talk
My name is Geoff Smith from the School of Pharmacy, De Montfort University, Leicester
I have been working for approximately 10 years
(click) on the development of P.A.T. solutions for pharmaceutical freeze-drying
(click) with electrical impedance spectroscopy being my primary focus

## Slide 2: Overview
Lyophilization
Benefits : Challenges
  Z-FDM
  Impedance-enabled
  freeze-drying microscopy
  Formulation development
  TVIS
  Through-vial impedance spectroscopy
Process development
Electrical Impedance Spectroscopy Process Analytical Technology
Design space solutions ……
Notes: I will start the talk with a few slides on why we need to freeze-dry certain drugs
and what are the benefits and challenges
before addressing the main focus of my talk
(Click) Which is the development of design space solutions based on eisPAT
(click) The first is an impedance-enabled freeze-drying microscope called Z-FDM
Which can be used for formulation development
(click) The second is through-vial impedance spectroscopy (or TVIS)
which uses the product container to support the electrode system
and can be used for process development

## Slide 3: Benefits of Lyophilization
Low moisture content
More surface area & porous
Easy to Dissolve
Powder
Increased Stability
Lyophilization
Freezing
Sublimation
Desorption
“40% of biologically based products have to be freeze dried”
“80% of the available products lyophilized in vial”
Zoster vaccine
(Zostavax®)
Azithromycin
injection.
(Zithromax®)
Easy to transport
Lyophilization commonly used for
  Small Molecules Drugs (e.g. penicillin)
  Large Molecule Drugs (e.g. proteins, DNA)
  Microorganisms (e.g. bacteria, virusus)
  Blood products
Notes: It is interesting to note how widely freeze-drying is used
across the biopharmaceutical industry
with approximately 40% of biological products requiring freeze-drying
for shelf-life purposes
And with the vast majority of these products being lyophilised in glass vials
which are then easy to transport
(Click) The process converts the liquid water to ice by freezing
then removes that by sublimation (at low temperature under a vacuum)
and finally heats the product to desorb a large proportion of moisture in the solid
(click) What results is a powder with low moisture content
and a high porosity that helps the solid to dissolve quickly
on reconstitution with water

## Slide 4: Applications (in the news) …… Remdesivir
Covid 19 therapies and vaccines
Re-purposed experimental drug treatment for Covid-19
co-formulated with cyclodextrin for solubility
& freeze-dried
Developed for Ebola (2008)
Notes: A freeze-dried drug that has been in the news recently
is Remdesivir from Gilead Sciences
It is a nucleotide analog with broad-spectrum antiviral activity
that was originally developed for Ebola treatment
(Click) but is now being re-purposed
as an experimental drug treatment for Covid-19.
(click) An interesting feature of this product
is that the poor solubility of the API
was addressed by formulating with a cyclo-dextrin
which solubilises the hydrophobic part of the molecule
Allowing an aqueous solution to be freeze-dried

## Slide 5: Challenges of Lyophilization
Complex 3 stage process
Cost: energy & GMP Long process (up to 5 days)
Difficult to scale-up
Variation within batch
Notes: As with many things ……. There’s always a down side
These can be summarised,
(click) firstly in terms of the complex nature of the process in which the three stages of freezing, primary drying and secondary drying are intimately linked
(click) Secondly, in terms of the energy cost and GMP footprint whereby large volumes of drug product solution have to be first frozen before removing the ice at a low temperature in a long primary drying stage;
(click) Thirdly, in terms of the challenges of scale up as the physics of heat and mass transfer differs between scales;
(click) and finally in terms of the variation within a batch that results from the heterogeneity in the heat and mass transfer across the dryer.

## Slide 6: Complex design space
Stability (chemical & physical)
  Packaging compatibility
  Critical product temperature
Lyophilization (Process Design)
Formulation (Product Design)
Freezing
Annealing
1° Drying
2° Drying
cooling rate
↓
↓
Ice crystal
structures
Process parameters
and
+
temperature
ramp
Final moisture
content
Shelf temperature
& hold time
↓
Maximize ice
crystal size
Notes: We can see the complexity of the process when we consider the design space:
[click 1] where formulation choices must deliver
chemical and physical stability
and compatibility with the primary container, in both the liquid and solid states
[click 2] while being mindful of the impact of formulation on
the product-specific critical temperature known as the collapse temperature Tc)
[click 3] then there are the process parameters of each of the 4 stages of the process
[click 4] where cooling rates and ice nucleation temperatures
Impact ice-growth and therefore the resulting crystalline matrix
[click 5] AND where an optional annealing process
might be used to maximise ice crystal sizes [CLICK]
That ultimately define the dry-layer resistance-to-vapour-flow (Rp)
[click 7] Then a combination of the dry layer resistance Rp , the temperature of the shelf Ts
and the heat transfer of coefficient of the vial Kv
[click 8] conspire together to define the rate of drying and the ice interface temperature Tp
[click 8] Which needs to stay below the collapse temperature Tc
in order to avoid product failure
[click 9] Note that Kv is impacted by the chamber pressure owing to gas conduction effects
[click] in the last stage (i.e. secondary drying)
[click] the shelf temperature is ramped
to deliver sufficient heat to desorb the surface water from the dry layer
[click] At a rate that ensures the product temperature again stays below the collapse temperature
In the expectation that a final moisture content is obtained
[click] that provides for chemical and physical stability

## Slide 7: Louis Rey 1960s
Rey (1960) Study of freezing and drying of tissues at very low temperatures. In Parkes and Audrey eds. Recent research in freezing and drying, Blackwell, Oxford.
Notes: …….. And so how do we use impedance analysis in lyo cycle development?
One of the first applications was demonstrated by Louis Rey in the 1960s

## Slide 8: Lyotherm Biopharma Process Systems
Integrated within cryostat
Pin electrode (pair)
Impedance analysis (Zsinφ ) at a single frequency (1 kHz) with
differential thermal analysis (DTA)
Ward & Matejtschuk , 2010 in Freeze Drying/ Lyophilization of Pharmaceutical & Biological Products 3rd ed. Rey,L & May JC eds, Informa Press, New York
Designed to measure temperatures
relevant to freeze-dried formulations
glass transition (TG’)
ice melting (TM) and eutectic (TEU)
Notes: and is now embodied in the Lyotherm instrument from Biopharma
This system combines
an electrical impedance measurement at a single excitation frequency of 1 kHz
with a differential thermal analyser
(Click) It’s used for the determination of product specific temperatures,
including the glass transition, and melting points
associated with ice and any crystalline solutes such as mannitol

## Slide 9: Dielectric loss or dielectric permittivity analysis?
Electrical Impedance Spectroscopy Process Analytical Technology
Design space solutions ……
Test object is measured at a range of discrete frequencies
Notes: What I’d like to do next
is to profile some of the applications for eisPAT
in the development of the design space
With a spectroscopic method
the impedance of the test object is measured at a range of discrete frequencies
[click]
in order to build the spectral response
This differentiates our approach from a single frequency measurement used in Lyotherm and LyoRx

## Slide 10: Dielectric loss or dielectric permittivity analysis?
Electrical Impedance Spectroscopy Process Analytical Technology
Design space solutions ……
  Novocontrol BDS
  Broad Band Dielectric Spectroscopy (sub Hertz to 10 MHz)
Test object is measured at a range of discrete frequencies
  IDE
  Inter-digitated electrodes
  Micro-sample measurement
  Formulation development
  TVIS
  Through-vial impedance spectroscopy for in vial measurement
Process development
Notes: There are very good commercial systems on the market for such measurements,
for example the Novocontrol range of broadband dielectric spectrometers
And so firstly, I wanted to describe how these can be modified for either
(click) micro-sample analysis using commercially available interdigitated electrodes for formulation development
(click) or for in-vial determination of critical temperatures on more process representative samples volumes

## Slide 11: Spectroscopy Systems (sub Hz to 10 MHz)
Novocontrol
BDS system
Novocontrol
BDS system
Notes: Here on the left is the Novocontrol BDS system with the sample holder and the active head of the spectrometer on suspended on a rack
…. (click)

## Slide 12: Spectroscopy Systems (sub Hz to 10 MHz)
Novocontrol
BDS system
Notes: To the right of the spectrometer is the cryostat (click)
with its liquid nitrogen Dewar

## Slide 13: Spectroscopy Systems (sub Hz to 10 MHz)
Cover
slip
Adapter -spacer
OPTION 1 Inter-digitated microelectrode array
IDE: 2 μL volume
Placed on a cradle
IDE
Notes: on the left you can see one of the IDEs (click)
These were sourced from a company called Micrux in Spain
In order to make the measurement we have designed
(click) an adapter to hold the IDE
Which also creates a sample space when the cover slip is placed on top
(click) because the adapter-spacer is approx 10 microns thicker than the IDE glass substrate
We then place that on a cradle (click) which is then lowered into the cryostat
(click)

## Slide 14: Spectroscopy Systems (sub Hz to 10 MHz)
OPTION 2 TVIS vial 2-3 ml volume
Placed on the cryostat “cradle”
Copper
foil
electrodes
Notes: In the next system we have a standard vial with electrodes attached to the outside (click)
Which again is also placed on the cradle (click) and lowered into the cryostat (click)

## Slide 15: The story so far ……..
Note that the technologies described so far are only capable of measurements during freeze-thawing cycles
A bit like a DSC style measurement
Notes: Note that the technologies described so far
are only capable of measurements during freeze-thawing cycles
Which is a bit like one has in a DSC style measurement

## Slide 16: Dielectric loss or dielectric permittivity analysis?
Electrical Impedance Spectroscopy Process Analytical Technology
Design space solutions ……
  Bespoke instrumentation
  Integrated within freeze-drying platforms
  Z-FDM
  Impedance-enabled
  freeze-drying microscopy
  Formulation development
  TVIS
  Through-vial impedance spectroscopy
Process development
Notes: The freeze-drying applications we have studied so far
Required the development of bespoke instrumentation (click)
in order to be able to measure the sample during an actual lyophilisation cycle.
(click) Most of the work to date has concerned the TVIS technology that was developed via various Innovate UK project grants
(click) It is only recently, in the last two years, that we started to develop the Z-FDM technology with our partner Biopharma Process Systems

## Slide 17: Spectroscopy Systems : TVIS
vial
Placed within the dryer
TVIS (Through-Vial Impedance Spectroscopy)
Junction box
Pass through
spectrometer
Modified glass vial
Notes: So first up is the TVIS system
(click) with the modified glass vial carrying the measurement electrodes
(click) which is placed inside the dryer
(click) and then connected to the junction box
(click) which then connects to the spectrometer outside the dryer
(click) via a pass-through on one of the existing ports of the dryer

## Slide 18: Spectroscopy Systems : Z-FDM
Developed in partnership with Biopharma Process Systems
on Innovate UK funded FAstLyo project ref. 133425 (2018-19)
Integrated within the FDM stage
Inter-digitated electrode
Notes: Next is the freeze-drying microscope Z-FDM
(click) with an integrated IDE system,
(click) again based on the Micrux electrode arrays

## Slide 19: Dielectric Loss Mechanisms
The polarization of the water dipole in liquid water at 20 ˚C, with a dielectric loss peak frequency of ~ 18 GHz
Chart: Log Frequency
| 6 | 5.9030899869919438 | 5.8239109124113 | 5.7569630370485534 | 5.6020599913279625 | 5.5228744023138034 | 5.4259741609193757 | 5.3010299956639813 | 5.204119982655925 | 5.1106906972737542 | 5 | 4.9030899869919438 | 4.8027190075796815 | 4.7044336600521994 | 4.6020599913279625 | 4.5016890119157003 | 4.4006588497649739 | 4.3010299956639813 | 4.200659016251719 | 4.1009905230699646 | 4 | 3.90049275542937 | 3.800655228145212 | 3.7000543856282389 | 3.6003302305807652 | 3.5003188237463867 | 3.4001233554370809 | 3.3001605369513523 | 3.2001388538573807 | 3.1000257301078626 | 3 | 2.9000611027354806 | 2.8000362418279794 | 2.7000023971422538 | 2.6000249038929866 | 2.5000030680516931 | 2.4000023459279558 | 2.3000082025538129 | 2.2000018654066018 | 2.0999912335446846 | 2 | 1.9000009651534695 | 1.8000018278179688 | 1.700002397142254 | 1.6000030866277404 | 1.5000030680516931 | 1.400002345927956 | 1.3000082025538131 | 1.2000018654066018 | 1.0999912335446844 | 1
Time 0.23 h, 20.3 celcius | 1.0162 | 1.0162 | 1.0162 | 1.0162 | 1.0176 | 1.024 | 1.0293 | 1.0371 | 1.0465 | 1.0575 | 1.0742 | 1.0971 | 1.131 | 1.18 | 1.2538 | 1.3532 | 1.4803 | 1.6281 | 1.7827 | 1.9288 | 2.0567 | 2.1587 | 2.2374 | 2.2971 | 2.3414 | 2.3756 | 2.4038 | 2.4272 | 2.4476 | 2.4662 | 2.4852 | 2.5003 | 2.5152 | 2.5286 | 2.5419 | 2.5531 | 2.5615 | 2.5717 | 2.5802 | 2.589 | 2.5992 | 2.6061 | 2.6201 | 2.625 | 2.6478 | 2.6645 | 2.686 | 2.708 | 2.7359 | 2.7645 | 2.7969
Time 5.03 h, -20 celcius | 0.084287 | 0.084287 | 0.084287 | 0.084287 | 0.083003 | 0.084127 | 0.084469 | 0.085543 | 0.086743 | 0.087572 | 0.088047 | 0.088435 | 0.088561 | 0.088505 | 0.088289 | 0.08811 | 0.08822 | 0.08935 | 0.092855 | 0.10126 | 0.11875 | 0.15045 | 0.2025 | 0.28088 | 0.38519 | 0.51085 | 0.64628 | 0.77735 | 0.89303 | 0.98847 | 1.0619 | 1.1159 | 1.155 | 1.183 | 1.203 | 1.2167 | 1.2267 | 1.2373 | 1.2444 | 1.2521 | 1.2603 | 1.2702 | 1.2796 | 1.2944 | 1.3089 | 1.3285 | 1.3531 | 1.3812 | 1.4143 | 1.4539 | 1.499
Time 8.5 h, -40 celcius | 0.083695 | 0.083695 | 0.083695 | 0.083695 | 0.083695 | 0.08324 | 0.083622 | 0.083847 | 0.084834 | 0.086128 | 0.086714 | 0.087381 | 0.087886 | 0.088558 | 0.089009 | 0.089429 | 0.089952 | 0.090576 | 0.09152 | 0.092833 | 0.094685 | 0.097293 | 0.10083 | 0.10562 | 0.11226 | 0.12153 | 0.13502 | 0.15512 | 0.18502 | 0.22832 | 0.28819 | 0.36571 | 0.45912 | 0.56375 | 0.67242 | 0.77798 | 0.87404 | 0.95702 | 1.0284 | 1.0845 | 1.1268 | 1.1614 | 1.1873 | 1.2052 | 1.2167 | 1.2287 | 1.2359 | 1.2394 | 1.2468 | 1.2512 | 1.2552 | 1.2597
Std. : Water (1:0)_ 5 g_17C | 2.3304 | 2.4387 | 2.4947 | 2.5334 | 2.5734 | 2.595 | 2.6101 | 2.6237 | 2.6363 | 2.6458 | 2.6525 | 2.6605 | 2.6675 | 2.6754 | 2.6841 | 2.6936 | 2.7028 | 2.7121 | 2.7221 | 2.732 | 2.7416 | 2.7519 | 2.7627 | 2.773 | 2.7842 | 2.7949 | 2.8043 | 2.8148 | 2.8246 | 2.8354 | 2.8466 | 2.8598 | 2.8739 | 2.8899 | 2.908 | 2.9285 | 2.9493 | 2.972 | 2.9971 | 3.0212 | 3.0504 | 3.076 | 3.1069 | 3.1381 | 3.1714 | 3.2072 | 3.2459 | 3.2864
Std. : Water (1:3)_5 g_22.3C | 1.4671 | 1.6855 | 1.744 | 1.8824 | 1.9929 | 2.1292 | 2.3085 | 2.4363 | 2.5381 | 2.631 | 2.6959 | 2.7426 | 2.7767 | 2.8037 | 2.8219 | 2.8373 | 2.8512 | 2.8646 | 2.8761 | 2.8875 | 2.8997 | 2.9118 | 2.9235 | 2.9355 | 2.9478 | 2.9606 | 2.9734 | 2.9866 | 2.9991 | 3.0123 | 3.0249 | 3.039 | 3.0531 | 3.0685 | 3.0846 | 3.1036 | 3.1223 | 3.1442 | 3.1674 | 3.1919 | 3.2199 | 3.2461 | 3.2797 | 3.3073 | 3.3426 | 3.3775 | 3.4158 | 3.4569 | 3.5017 | 3.5489
Fitting-Time 0.23 h (20.3 C) Liquid | 2.412 | 2.412 | 2.412 | 2.412 | 2.412 | 2.412 | 2.412 | 2.412 | 2.412 | 2.4119 | 2.4119 | 2.4119 | 2.4119 | 2.4118 | 2.4117 | 2.4115 | 2.4112 | 2.4108 | 2.4101 | 2.409 | 2.4073 | 2.4046 | 2.4004 | 2.3937 | 2.3832 | 2.367 | 2.342 | 2.3043 | 2.2484 | 2.1697 | 2.0642 | 1.9301 | 1.7781 | 1.6192 | 1.4715 | 1.3445 | 1.2461 | 1.1731 | 1.1243 | 1.0907 | 1.0692 | 1.0535 | 1.0451 | 1.0395 | 1.035 | 1.0329 | 1.0318 | 1.0305 | 1.0302 | 1.0299 | 1.0297
Fitting-Time 5.03 h (-20 C) Frozen | 1.2389 | 1.2389 | 1.2389 | 1.2389 | 1.2388 | 1.2387 | 1.2386 | 1.2384 | 1.2381 | 1.2377 | 1.2369 | 1.2358 | 1.2339 | 1.231 | 1.2264 | 1.2192 | 1.208 | 1.1906 | 1.1642 | 1.1248 | 1.0679 | 0.98926 | 0.88724 | 0.76529 | 0.63274 | 0.50242 | 0.38716 | 0.29408 | 0.22349 | 0.17372 | 0.13979 | 0.11692 | 0.10222 | 0.092682 | 0.086624 | 0.08272 | 0.080267 | 0.078693 | 0.077739 | 0.077121 | 0.076743 | 0.076474 | 0.076332 | 0.076237 | 0.076164 | 0.07613 | 0.076111 | 0.076089 | 0.076084 | 0.076079 | 0.076076
18 GHz
TVIS range
~ 80
~ 3
https://en.wikipedia.org/wiki/Permittivity
Real part Capacitance
Imaginary part Capacitance
Chart: Log Frequency
| 6 | 5.9030899869919438 | 5.8239109124113 | 5.7569630370485534 | 5.6020599913279625 | 5.5228744023138034 | 5.4259741609193757 | 5.3010299956639813 | 5.204119982655925 | 5.1106906972737542 | 5 | 4.9030899869919438 | 4.8027190075796815 | 4.7044336600521994 | 4.6020599913279625 | 4.5016890119157003 | 4.4006588497649739 | 4.3010299956639813 | 4.200659016251719 | 4.1009905230699646 | 4 | 3.90049275542937 | 3.800655228145212 | 3.7000543856282389 | 3.6003302305807652 | 3.5003188237463867 | 3.4001233554370809 | 3.3001605369513523 | 3.2001388538573807 | 3.1000257301078626 | 3 | 2.9000611027354806 | 2.8000362418279794 | 2.7000023971422538 | 2.6000249038929866 | 2.5000030680516931 | 2.4000023459279558 | 2.3000082025538129 | 2.2000018654066018 | 2.0999912335446846 | 2 | 1.9000009651534695 | 1.8000018278179688 | 1.700002397142254 | 1.6000030866277404 | 1.5000030680516931 | 1.400002345927956 | 1.3000082025538131 | 1.2000018654066018 | 1.0999912335446844 | 1
Time 0.23 h, 20.3 celcius | 0.021874 | 0.027746 | 0.035469 | 0.045629 | 0.058992 | 0.069416 | 0.087012 | 0.11672 | 0.14702 | 0.18167 | 0.23092 | 0.28348 | 0.3471 | 0.41787 | 0.49639 | 0.57052 | 0.6315 | 0.66609 | 0.66868 | 0.64015 | 0.58783 | 0.52385 | 0.45806 | 0.3962 | 0.3406 | 0.2936 | 0.25428 | 0.22269 | 0.19622 | 0.17597 | 0.15804 | 0.14279 | 0.13021 | 0.12053 | 0.11142 | 0.10593 | 0.099251 | 0.10112 | 0.096409 | 0.099903 | 0.099379 | 0.11049 | 0.12227 | 0.13167 | 0.14829 | 0.16415 | 0.18118 | 0.20571 | 0.22768 | 0.25157 | 0.27443
Time 5.03 h, -20 celcius | 0.0046903 | 0.0060276 | 0.0048957 | 0.0052689 | 0.0080706 | 0.0070995 | 0.0085621 | 0.011385 | 0.014441 | 0.017939 | 0.023068 | 0.028754 | 0.036271 | 0.045614 | 0.058069 | 0.073874 | 0.094576 | 0.12111 | 0.15588 | 0.20027 | 0.2566 | 0.32289 | 0.39693 | 0.47149 | 0.53464 | 0.57592 | 0.58749 | 0.56901 | 0.52696 | 0.47094 | 0.40966 | 0.35018 | 0.29633 | 0.24993 | 0.21217 | 0.18272 | 0.16189 | 0.14492 | 0.13366 | 0.12856 | 0.12752 | 0.12988 | 0.13813 | 0.14441 | 0.16577 | 0.18416 | 0.20379 | 0.22754 | 0.25211 | 0.27626 | 0.29768
Time 8.5 h, -40 celcius | 0.0037257 | 0.0037257 | 0.0022099 | 0.0055149 | 0.0027352 | 0.0046061 | 0.0028107 | 0.0031095 | 0.0040131 | 0.0050574 | 0.0061923 | 0.007861 | 0.0096387 | 0.01196 | 0.014763 | 0.018394 | 0.022849 | 0.028488 | 0.035374 | 0.043956 | 0.054453 | 0.067485 | 0.083211 | 0.10248 | 0.12627 | 0.15518 | 0.19059 | 0.23316 | 0.28257 | 0.33712 | 0.39303 | 0.44437 | 0.48479 | 0.5087 | 0.51347 | 0.50011 | 0.47159 | 0.43276 | 0.38638 | 0.3379 | 0.29199 | 0.24717 | 0.21022 | 0.17522 | 0.14921 | 0.12645 | 0.10764 | 0.094062 | 0.085294 | 0.077832 | 0.076166 | 0.074374
Std. : Water (1:0)_ 5 g_17C | 0.40745 | 0.37758 | 0.33167 | 0.27797 | 0.22443 | 0.19417 | 0.16169 | 0.13849 | 0.12143 | 0.10697 | 0.096405 | 0.087034 | 0.081871 | 0.078656 | 0.076272 | 0.075226 | 0.07448 | 0.073601 | 0.073296 | 0.073701 | 0.074654 | 0.075483 | 0.075353 | 0.07631 | 0.0769 | 0.077719 | 0.079173 | 0.081297 | 0.084848 | 0.090883 | 0.098449 | 0.10715 | 0.11892 | 0.13057 | 0.14131 | 0.15224 | 0.161 | 0.1718 | 0.18315 | 0.19373 | 0.20789 | 0.22266 | 0.23803 | 0.25543 | 0.2743 | 0.29629 | 0.32039 | 0.34659
Std. : Water (1:3)_5 g_22.3C | 0.35022 | 0.37378 | 0.41173 | 0.55328 | 0.59494 | 0.61621 | 0.60526 | 0.57334 | 0.52449 | 0.45124 | 0.3927 | 0.33463 | 0.28521 | 0.24069 | 0.2067 | 0.17971 | 0.15895 | 0.14354 | 0.13098 | 0.1209 | 0.11373 | 0.10865 | 0.10508 | 0.10263 | 0.10025 | 0.099388 | 0.099009 | 0.09943 | 0.10029 | 0.10249 | 0.10653 | 0.11105 | 0.11816 | 0.12566 | 0.13766 | 0.14944 | 0.16023 | 0.17158 | 0.18231 | 0.19465 | 0.20803 | 0.22162 | 0.23412 | 0.25639 | 0.27568 | 0.29801 | 0.32242 | 0.35086 | 0.38221 | 0.41669
Fitting-Time 0.23 h (20.3 C) Liquid | 0.00080148 | 0.001009 | 0.0012703 | 0.0015992 | 0.0020132 | 0.0025345 | 0.0031908 | 0.0040169 | 0.005057 | 0.0063663 | 0.0080146 | 0.010089 | 0.012702 | 0.01599 | 0.020128 | 0.025337 | 0.031892 | 0.040136 | 0.050507 | 0.063538 | 0.07988 | 0.10037 | 0.126 | 0.15786 | 0.1972 | 0.24538 | 0.30315 | 0.37047 | 0.44655 | 0.52567 | 0.59992 | 0.65886 | 0.68897 | 0.68388 | 0.64493 | 0.58011 | 0.50283 | 0.42213 | 0.34988 | 0.28493 | 0.23165 | 0.18163 | 0.14738 | 0.11839 | 0.089082 | 0.071374 | 0.059526 | 0.041708 | 0.035758 | 0.029805 | 0.023848
Fitting-Time 5.03 h (-20 C) Frozen | 0.0048296 | 0.0060799 | 0.0076542 | 0.0096359 | 0.01213 | 0.01527 | 0.019222 | 0.024195 | 0.030452 | 0.038322 | 0.048213 | 0.060635 | 0.076215 | 0.095709 | 0.12001 | 0.15014 | 0.18717 | 0.232 | 0.28517 | 0.34602 | 0.41191 | 0.4775 | 0.53412 | 0.57135 | 0.58091 | 0.56037 | 0.51476 | 0.45386 | 0.38691 | 0.32252 | 0.26465 | 0.2141 | 0.17243 | 0.138 | 0.11029 | 0.087693 | 0.069745 | 0.055173 | 0.044035 | 0.034967 | 0.027983 | 0.021692 | 0.017495 | 0.013998 | 0.010499 | 0.0083994 | 0.0069995 | 0.0048997 | 0.0041998 | 0.0034999 | 0.0027999
(I)
Notes: Having described the various hardware systems
Next I’d like to give an overview of the
wide range of processes that can be measured
The first process
which the dielectric relaxation of liquid water
can not be measured with the systems I have described
However, its worth mentioning
because there is a similar process for ice
that I will come onto later

## Slide 20: Dielectric Loss Mechanisms
Maxwell-Wagner (MW) polarization of the glass wall of the TVIS vial at +20 ˚C, with a dielectric loss peak frequency of 17.8 kHz
Chart: Log Frequency
| 6 | 5.9030899869919438 | 5.8239109124113 | 5.7569630370485534 | 5.6020599913279625 | 5.5228744023138034 | 5.4259741609193757 | 5.3010299956639813 | 5.204119982655925 | 5.1106906972737542 | 5 | 4.9030899869919438 | 4.8027190075796815 | 4.7044336600521994 | 4.6020599913279625 | 4.5016890119157003 | 4.4006588497649739 | 4.3010299956639813 | 4.200659016251719 | 4.1009905230699646 | 4 | 3.90049275542937 | 3.800655228145212 | 3.7000543856282389 | 3.6003302305807652 | 3.5003188237463867 | 3.4001233554370809 | 3.3001605369513523 | 3.2001388538573807 | 3.1000257301078626 | 3 | 2.9000611027354806 | 2.8000362418279794 | 2.7000023971422538 | 2.6000249038929866 | 2.5000030680516931 | 2.4000023459279558 | 2.3000082025538129 | 2.2000018654066018 | 2.0999912335446846 | 2 | 1.9000009651534695 | 1.8000018278179688 | 1.700002397142254 | 1.6000030866277404 | 1.5000030680516931 | 1.400002345927956 | 1.3000082025538131 | 1.2000018654066018 | 1.0999912335446844 | 1
Time 0.23 h, 20.3 celcius | 1.0162 | 1.0162 | 1.0162 | 1.0162 | 1.0176 | 1.024 | 1.0293 | 1.0371 | 1.0465 | 1.0575 | 1.0742 | 1.0971 | 1.131 | 1.18 | 1.2538 | 1.3532 | 1.4803 | 1.6281 | 1.7827 | 1.9288 | 2.0567 | 2.1587 | 2.2374 | 2.2971 | 2.3414 | 2.3756 | 2.4038 | 2.4272 | 2.4476 | 2.4662 | 2.4852 | 2.5003 | 2.5152 | 2.5286 | 2.5419 | 2.5531 | 2.5615 | 2.5717 | 2.5802 | 2.589 | 2.5992 | 2.6061 | 2.6201 | 2.625 | 2.6478 | 2.6645 | 2.686 | 2.708 | 2.7359 | 2.7645 | 2.7969
Time 5.03 h, -20 celcius | 0.084287 | 0.084287 | 0.084287 | 0.084287 | 0.083003 | 0.084127 | 0.084469 | 0.085543 | 0.086743 | 0.087572 | 0.088047 | 0.088435 | 0.088561 | 0.088505 | 0.088289 | 0.08811 | 0.08822 | 0.08935 | 0.092855 | 0.10126 | 0.11875 | 0.15045 | 0.2025 | 0.28088 | 0.38519 | 0.51085 | 0.64628 | 0.77735 | 0.89303 | 0.98847 | 1.0619 | 1.1159 | 1.155 | 1.183 | 1.203 | 1.2167 | 1.2267 | 1.2373 | 1.2444 | 1.2521 | 1.2603 | 1.2702 | 1.2796 | 1.2944 | 1.3089 | 1.3285 | 1.3531 | 1.3812 | 1.4143 | 1.4539 | 1.499
Time 8.5 h, -40 celcius | 0.083695 | 0.083695 | 0.083695 | 0.083695 | 0.083695 | 0.08324 | 0.083622 | 0.083847 | 0.084834 | 0.086128 | 0.086714 | 0.087381 | 0.087886 | 0.088558 | 0.089009 | 0.089429 | 0.089952 | 0.090576 | 0.09152 | 0.092833 | 0.094685 | 0.097293 | 0.10083 | 0.10562 | 0.11226 | 0.12153 | 0.13502 | 0.15512 | 0.18502 | 0.22832 | 0.28819 | 0.36571 | 0.45912 | 0.56375 | 0.67242 | 0.77798 | 0.87404 | 0.95702 | 1.0284 | 1.0845 | 1.1268 | 1.1614 | 1.1873 | 1.2052 | 1.2167 | 1.2287 | 1.2359 | 1.2394 | 1.2468 | 1.2512 | 1.2552 | 1.2597
Std. : Water (1:0)_ 5 g_17C | 2.3304 | 2.4387 | 2.4947 | 2.5334 | 2.5734 | 2.595 | 2.6101 | 2.6237 | 2.6363 | 2.6458 | 2.6525 | 2.6605 | 2.6675 | 2.6754 | 2.6841 | 2.6936 | 2.7028 | 2.7121 | 2.7221 | 2.732 | 2.7416 | 2.7519 | 2.7627 | 2.773 | 2.7842 | 2.7949 | 2.8043 | 2.8148 | 2.8246 | 2.8354 | 2.8466 | 2.8598 | 2.8739 | 2.8899 | 2.908 | 2.9285 | 2.9493 | 2.972 | 2.9971 | 3.0212 | 3.0504 | 3.076 | 3.1069 | 3.1381 | 3.1714 | 3.2072 | 3.2459 | 3.2864
Std. : Water (1:3)_5 g_22.3C | 1.4671 | 1.6855 | 1.744 | 1.8824 | 1.9929 | 2.1292 | 2.3085 | 2.4363 | 2.5381 | 2.631 | 2.6959 | 2.7426 | 2.7767 | 2.8037 | 2.8219 | 2.8373 | 2.8512 | 2.8646 | 2.8761 | 2.8875 | 2.8997 | 2.9118 | 2.9235 | 2.9355 | 2.9478 | 2.9606 | 2.9734 | 2.9866 | 2.9991 | 3.0123 | 3.0249 | 3.039 | 3.0531 | 3.0685 | 3.0846 | 3.1036 | 3.1223 | 3.1442 | 3.1674 | 3.1919 | 3.2199 | 3.2461 | 3.2797 | 3.3073 | 3.3426 | 3.3775 | 3.4158 | 3.4569 | 3.5017 | 3.5489
Fitting-Time 0.23 h (20.3 C) Liquid | 2.412 | 2.412 | 2.412 | 2.412 | 2.412 | 2.412 | 2.412 | 2.412 | 2.412 | 2.4119 | 2.4119 | 2.4119 | 2.4119 | 2.4118 | 2.4117 | 2.4115 | 2.4112 | 2.4108 | 2.4101 | 2.409 | 2.4073 | 2.4046 | 2.4004 | 2.3937 | 2.3832 | 2.367 | 2.342 | 2.3043 | 2.2484 | 2.1697 | 2.0642 | 1.9301 | 1.7781 | 1.6192 | 1.4715 | 1.3445 | 1.2461 | 1.1731 | 1.1243 | 1.0907 | 1.0692 | 1.0535 | 1.0451 | 1.0395 | 1.035 | 1.0329 | 1.0318 | 1.0305 | 1.0302 | 1.0299 | 1.0297
Fitting-Time 5.03 h (-20 C) Frozen | 1.2389 | 1.2389 | 1.2389 | 1.2389 | 1.2388 | 1.2387 | 1.2386 | 1.2384 | 1.2381 | 1.2377 | 1.2369 | 1.2358 | 1.2339 | 1.231 | 1.2264 | 1.2192 | 1.208 | 1.1906 | 1.1642 | 1.1248 | 1.0679 | 0.98926 | 0.88724 | 0.76529 | 0.63274 | 0.50242 | 0.38716 | 0.29408 | 0.22349 | 0.17372 | 0.13979 | 0.11692 | 0.10222 | 0.092682 | 0.086624 | 0.08272 | 0.080267 | 0.078693 | 0.077739 | 0.077121 | 0.076743 | 0.076474 | 0.076332 | 0.076237 | 0.076164 | 0.07613 | 0.076111 | 0.076089 | 0.076084 | 0.076079 | 0.076076
Chart: Log Frequency
| 6 | 5.9030899869919438 | 5.8239109124113 | 5.7569630370485534 | 5.6020599913279625 | 5.5228744023138034 | 5.4259741609193757 | 5.3010299956639813 | 5.204119982655925 | 5.1106906972737542 | 5 | 4.9030899869919438 | 4.8027190075796815 | 4.7044336600521994 | 4.6020599913279625 | 4.5016890119157003 | 4.4006588497649739 | 4.3010299956639813 | 4.200659016251719 | 4.1009905230699646 | 4 | 3.90049275542937 | 3.800655228145212 | 3.7000543856282389 | 3.6003302305807652 | 3.5003188237463867 | 3.4001233554370809 | 3.3001605369513523 | 3.2001388538573807 | 3.1000257301078626 | 3 | 2.9000611027354806 | 2.8000362418279794 | 2.7000023971422538 | 2.6000249038929866 | 2.5000030680516931 | 2.4000023459279558 | 2.3000082025538129 | 2.2000018654066018 | 2.0999912335446846 | 2 | 1.9000009651534695 | 1.8000018278179688 | 1.700002397142254 | 1.6000030866277404 | 1.5000030680516931 | 1.400002345927956 | 1.3000082025538131 | 1.2000018654066018 | 1.0999912335446844 | 1
Time 0.23 h, 20.3 celcius | 0.021874 | 0.027746 | 0.035469 | 0.045629 | 0.058992 | 0.069416 | 0.087012 | 0.11672 | 0.14702 | 0.18167 | 0.23092 | 0.28348 | 0.3471 | 0.41787 | 0.49639 | 0.57052 | 0.6315 | 0.66609 | 0.66868 | 0.64015 | 0.58783 | 0.52385 | 0.45806 | 0.3962 | 0.3406 | 0.2936 | 0.25428 | 0.22269 | 0.19622 | 0.17597 | 0.15804 | 0.14279 | 0.13021 | 0.12053 | 0.11142 | 0.10593 | 0.099251 | 0.10112 | 0.096409 | 0.099903 | 0.099379 | 0.11049 | 0.12227 | 0.13167 | 0.14829 | 0.16415 | 0.18118 | 0.20571 | 0.22768 | 0.25157 | 0.27443
Time 5.03 h, -20 celcius | 0.0046903 | 0.0060276 | 0.0048957 | 0.0052689 | 0.0080706 | 0.0070995 | 0.0085621 | 0.011385 | 0.014441 | 0.017939 | 0.023068 | 0.028754 | 0.036271 | 0.045614 | 0.058069 | 0.073874 | 0.094576 | 0.12111 | 0.15588 | 0.20027 | 0.2566 | 0.32289 | 0.39693 | 0.47149 | 0.53464 | 0.57592 | 0.58749 | 0.56901 | 0.52696 | 0.47094 | 0.40966 | 0.35018 | 0.29633 | 0.24993 | 0.21217 | 0.18272 | 0.16189 | 0.14492 | 0.13366 | 0.12856 | 0.12752 | 0.12988 | 0.13813 | 0.14441 | 0.16577 | 0.18416 | 0.20379 | 0.22754 | 0.25211 | 0.27626 | 0.29768
Time 8.5 h, -40 celcius | 0.0037257 | 0.0037257 | 0.0022099 | 0.0055149 | 0.0027352 | 0.0046061 | 0.0028107 | 0.0031095 | 0.0040131 | 0.0050574 | 0.0061923 | 0.007861 | 0.0096387 | 0.01196 | 0.014763 | 0.018394 | 0.022849 | 0.028488 | 0.035374 | 0.043956 | 0.054453 | 0.067485 | 0.083211 | 0.10248 | 0.12627 | 0.15518 | 0.19059 | 0.23316 | 0.28257 | 0.33712 | 0.39303 | 0.44437 | 0.48479 | 0.5087 | 0.51347 | 0.50011 | 0.47159 | 0.43276 | 0.38638 | 0.3379 | 0.29199 | 0.24717 | 0.21022 | 0.17522 | 0.14921 | 0.12645 | 0.10764 | 0.094062 | 0.085294 | 0.077832 | 0.076166 | 0.074374
Std. : Water (1:0)_ 5 g_17C | 0.40745 | 0.37758 | 0.33167 | 0.27797 | 0.22443 | 0.19417 | 0.16169 | 0.13849 | 0.12143 | 0.10697 | 0.096405 | 0.087034 | 0.081871 | 0.078656 | 0.076272 | 0.075226 | 0.07448 | 0.073601 | 0.073296 | 0.073701 | 0.074654 | 0.075483 | 0.075353 | 0.07631 | 0.0769 | 0.077719 | 0.079173 | 0.081297 | 0.084848 | 0.090883 | 0.098449 | 0.10715 | 0.11892 | 0.13057 | 0.14131 | 0.15224 | 0.161 | 0.1718 | 0.18315 | 0.19373 | 0.20789 | 0.22266 | 0.23803 | 0.25543 | 0.2743 | 0.29629 | 0.32039 | 0.34659
Std. : Water (1:3)_5 g_22.3C | 0.35022 | 0.37378 | 0.41173 | 0.55328 | 0.59494 | 0.61621 | 0.60526 | 0.57334 | 0.52449 | 0.45124 | 0.3927 | 0.33463 | 0.28521 | 0.24069 | 0.2067 | 0.17971 | 0.15895 | 0.14354 | 0.13098 | 0.1209 | 0.11373 | 0.10865 | 0.10508 | 0.10263 | 0.10025 | 0.099388 | 0.099009 | 0.09943 | 0.10029 | 0.10249 | 0.10653 | 0.11105 | 0.11816 | 0.12566 | 0.13766 | 0.14944 | 0.16023 | 0.17158 | 0.18231 | 0.19465 | 0.20803 | 0.22162 | 0.23412 | 0.25639 | 0.27568 | 0.29801 | 0.32242 | 0.35086 | 0.38221 | 0.41669
Fitting-Time 0.23 h (20.3 C) Liquid | 0.00080148 | 0.001009 | 0.0012703 | 0.0015992 | 0.0020132 | 0.0025345 | 0.0031908 | 0.0040169 | 0.005057 | 0.0063663 | 0.0080146 | 0.010089 | 0.012702 | 0.01599 | 0.020128 | 0.025337 | 0.031892 | 0.040136 | 0.050507 | 0.063538 | 0.07988 | 0.10037 | 0.126 | 0.15786 | 0.1972 | 0.24538 | 0.30315 | 0.37047 | 0.44655 | 0.52567 | 0.59992 | 0.65886 | 0.68897 | 0.68388 | 0.64493 | 0.58011 | 0.50283 | 0.42213 | 0.34988 | 0.28493 | 0.23165 | 0.18163 | 0.14738 | 0.11839 | 0.089082 | 0.071374 | 0.059526 | 0.041708 | 0.035758 | 0.029805 | 0.023848
Fitting-Time 5.03 h (-20 C) Frozen | 0.0048296 | 0.0060799 | 0.0076542 | 0.0096359 | 0.01213 | 0.01527 | 0.019222 | 0.024195 | 0.030452 | 0.038322 | 0.048213 | 0.060635 | 0.076215 | 0.095709 | 0.12001 | 0.15014 | 0.18717 | 0.232 | 0.28517 | 0.34602 | 0.41191 | 0.4775 | 0.53412 | 0.57135 | 0.58091 | 0.56037 | 0.51476 | 0.45386 | 0.38691 | 0.32252 | 0.26465 | 0.2141 | 0.17243 | 0.138 | 0.11029 | 0.087693 | 0.069745 | 0.055173 | 0.044035 | 0.034967 | 0.027983 | 0.021692 | 0.017495 | 0.013998 | 0.010499 | 0.0083994 | 0.0069995 | 0.0048997 | 0.0041998 | 0.0034999 | 0.0027999
18 GHz
20.3 °C
18 kHz
Real part Capacitance
Imaginary part Capacitance
Measurement vial
+
-
-
+
+
+
+
+
+
+
+
+
+
+
-
-
-
-
-
-
-
-
-
-
+
+
+
+
+
+
+
+
+
+
-
-
-
-
-
-
-
-
-
-
Water
Glass wall
Electronic polarization
Atomic polarization
o
H
H
δ-
δ+
δ+
Dipolar polarization
Grotthus mechanism
o
H
H
δ-
δ+
δ+
o
H
H
δ-
δ+
δ+
H
o
H
H
o
H
H
o
H
H+
Ionic diffusion
H+
HCO3−
Na+
Cl−
H+
H+
OH-
OH-
H+
(I)
(II)
20.3 °C
Application: Determine cell constant and
convert measured capacitance CS
to dielectric constant ε
Notes: The next process is unique to the TVIS measurement
and is caused by the polarization of the glass wall
through the conductivity of water within the vial
Is known as a Maxwell-Wagner or Interfacial charging process
[click] We have used this process to calibrate the system
in order to determine the cell constant of the vial
Once you have the cell constant then you can
convert measured capacitances into dielectric constant

## Slide 21: Dielectric Loss Mechanisms
Chart: Log Frequency
| 6 | 5.9030899869919438 | 5.8239109124113 | 5.7569630370485534 | 5.6020599913279625 | 5.5228744023138034 | 5.4259741609193757 | 5.3010299956639813 | 5.204119982655925 | 5.1106906972737542 | 5 | 4.9030899869919438 | 4.8027190075796815 | 4.7044336600521994 | 4.6020599913279625 | 4.5016890119157003 | 4.4006588497649739 | 4.3010299956639813 | 4.200659016251719 | 4.1009905230699646 | 4 | 3.90049275542937 | 3.800655228145212 | 3.7000543856282389 | 3.6003302305807652 | 3.5003188237463867 | 3.4001233554370809 | 3.3001605369513523 | 3.2001388538573807 | 3.1000257301078626 | 3 | 2.9000611027354806 | 2.8000362418279794 | 2.7000023971422538 | 2.6000249038929866 | 2.5000030680516931 | 2.4000023459279558 | 2.3000082025538129 | 2.2000018654066018 | 2.0999912335446846 | 2 | 1.9000009651534695 | 1.8000018278179688 | 1.700002397142254 | 1.6000030866277404 | 1.5000030680516931 | 1.400002345927956 | 1.3000082025538131 | 1.2000018654066018 | 1.0999912335446844 | 1
Time 0.23 h, 20.3 celcius | 1.0162 | 1.0162 | 1.0162 | 1.0162 | 1.0176 | 1.024 | 1.0293 | 1.0371 | 1.0465 | 1.0575 | 1.0742 | 1.0971 | 1.131 | 1.18 | 1.2538 | 1.3532 | 1.4803 | 1.6281 | 1.7827 | 1.9288 | 2.0567 | 2.1587 | 2.2374 | 2.2971 | 2.3414 | 2.3756 | 2.4038 | 2.4272 | 2.4476 | 2.4662 | 2.4852 | 2.5003 | 2.5152 | 2.5286 | 2.5419 | 2.5531 | 2.5615 | 2.5717 | 2.5802 | 2.589 | 2.5992 | 2.6061 | 2.6201 | 2.625 | 2.6478 | 2.6645 | 2.686 | 2.708 | 2.7359 | 2.7645 | 2.7969
Time 5.03 h, -20 celcius | 0.084287 | 0.084287 | 0.084287 | 0.084287 | 0.083003 | 0.084127 | 0.084469 | 0.085543 | 0.086743 | 0.087572 | 0.088047 | 0.088435 | 0.088561 | 0.088505 | 0.088289 | 0.08811 | 0.08822 | 0.08935 | 0.092855 | 0.10126 | 0.11875 | 0.15045 | 0.2025 | 0.28088 | 0.38519 | 0.51085 | 0.64628 | 0.77735 | 0.89303 | 0.98847 | 1.0619 | 1.1159 | 1.155 | 1.183 | 1.203 | 1.2167 | 1.2267 | 1.2373 | 1.2444 | 1.2521 | 1.2603 | 1.2702 | 1.2796 | 1.2944 | 1.3089 | 1.3285 | 1.3531 | 1.3812 | 1.4143 | 1.4539 | 1.499
Time 8.5 h, -40 celcius | 0.083695 | 0.083695 | 0.083695 | 0.083695 | 0.083695 | 0.08324 | 0.083622 | 0.083847 | 0.084834 | 0.086128 | 0.086714 | 0.087381 | 0.087886 | 0.088558 | 0.089009 | 0.089429 | 0.089952 | 0.090576 | 0.09152 | 0.092833 | 0.094685 | 0.097293 | 0.10083 | 0.10562 | 0.11226 | 0.12153 | 0.13502 | 0.15512 | 0.18502 | 0.22832 | 0.28819 | 0.36571 | 0.45912 | 0.56375 | 0.67242 | 0.77798 | 0.87404 | 0.95702 | 1.0284 | 1.0845 | 1.1268 | 1.1614 | 1.1873 | 1.2052 | 1.2167 | 1.2287 | 1.2359 | 1.2394 | 1.2468 | 1.2512 | 1.2552 | 1.2597
Std. : Water (1:0)_ 5 g_17C | 2.3304 | 2.4387 | 2.4947 | 2.5334 | 2.5734 | 2.595 | 2.6101 | 2.6237 | 2.6363 | 2.6458 | 2.6525 | 2.6605 | 2.6675 | 2.6754 | 2.6841 | 2.6936 | 2.7028 | 2.7121 | 2.7221 | 2.732 | 2.7416 | 2.7519 | 2.7627 | 2.773 | 2.7842 | 2.7949 | 2.8043 | 2.8148 | 2.8246 | 2.8354 | 2.8466 | 2.8598 | 2.8739 | 2.8899 | 2.908 | 2.9285 | 2.9493 | 2.972 | 2.9971 | 3.0212 | 3.0504 | 3.076 | 3.1069 | 3.1381 | 3.1714 | 3.2072 | 3.2459 | 3.2864
Std. : Water (1:3)_5 g_22.3C | 1.4671 | 1.6855 | 1.744 | 1.8824 | 1.9929 | 2.1292 | 2.3085 | 2.4363 | 2.5381 | 2.631 | 2.6959 | 2.7426 | 2.7767 | 2.8037 | 2.8219 | 2.8373 | 2.8512 | 2.8646 | 2.8761 | 2.8875 | 2.8997 | 2.9118 | 2.9235 | 2.9355 | 2.9478 | 2.9606 | 2.9734 | 2.9866 | 2.9991 | 3.0123 | 3.0249 | 3.039 | 3.0531 | 3.0685 | 3.0846 | 3.1036 | 3.1223 | 3.1442 | 3.1674 | 3.1919 | 3.2199 | 3.2461 | 3.2797 | 3.3073 | 3.3426 | 3.3775 | 3.4158 | 3.4569 | 3.5017 | 3.5489
Fitting-Time 0.23 h (20.3 C) Liquid | 2.412 | 2.412 | 2.412 | 2.412 | 2.412 | 2.412 | 2.412 | 2.412 | 2.412 | 2.4119 | 2.4119 | 2.4119 | 2.4119 | 2.4118 | 2.4117 | 2.4115 | 2.4112 | 2.4108 | 2.4101 | 2.409 | 2.4073 | 2.4046 | 2.4004 | 2.3937 | 2.3832 | 2.367 | 2.342 | 2.3043 | 2.2484 | 2.1697 | 2.0642 | 1.9301 | 1.7781 | 1.6192 | 1.4715 | 1.3445 | 1.2461 | 1.1731 | 1.1243 | 1.0907 | 1.0692 | 1.0535 | 1.0451 | 1.0395 | 1.035 | 1.0329 | 1.0318 | 1.0305 | 1.0302 | 1.0299 | 1.0297
Fitting-Time 5.03 h (-20 C) Frozen | 1.2389 | 1.2389 | 1.2389 | 1.2389 | 1.2388 | 1.2387 | 1.2386 | 1.2384 | 1.2381 | 1.2377 | 1.2369 | 1.2358 | 1.2339 | 1.231 | 1.2264 | 1.2192 | 1.208 | 1.1906 | 1.1642 | 1.1248 | 1.0679 | 0.98926 | 0.88724 | 0.76529 | 0.63274 | 0.50242 | 0.38716 | 0.29408 | 0.22349 | 0.17372 | 0.13979 | 0.11692 | 0.10222 | 0.092682 | 0.086624 | 0.08272 | 0.080267 | 0.078693 | 0.077739 | 0.077121 | 0.076743 | 0.076474 | 0.076332 | 0.076237 | 0.076164 | 0.07613 | 0.076111 | 0.076089 | 0.076084 | 0.076079 | 0.076076
Maxwell-Wagner (MW) polarization of the glass wall of the TVIS vial at +20 ˚C, with a dielectric loss peak frequency of 17.8 kHz
Chart: Log Frequency
| 6 | 5.9030899869919438 | 5.8239109124113 | 5.7569630370485534 | 5.6020599913279625 | 5.5228744023138034 | 5.4259741609193757 | 5.3010299956639813 | 5.204119982655925 | 5.1106906972737542 | 5 | 4.9030899869919438 | 4.8027190075796815 | 4.7044336600521994 | 4.6020599913279625 | 4.5016890119157003 | 4.4006588497649739 | 4.3010299956639813 | 4.200659016251719 | 4.1009905230699646 | 4 | 3.90049275542937 | 3.800655228145212 | 3.7000543856282389 | 3.6003302305807652 | 3.5003188237463867 | 3.4001233554370809 | 3.3001605369513523 | 3.2001388538573807 | 3.1000257301078626 | 3 | 2.9000611027354806 | 2.8000362418279794 | 2.7000023971422538 | 2.6000249038929866 | 2.5000030680516931 | 2.4000023459279558 | 2.3000082025538129 | 2.2000018654066018 | 2.0999912335446846 | 2 | 1.9000009651534695 | 1.8000018278179688 | 1.700002397142254 | 1.6000030866277404 | 1.5000030680516931 | 1.400002345927956 | 1.3000082025538131 | 1.2000018654066018 | 1.0999912335446844 | 1
Time 0.23 h, 20.3 celcius | 0.021874 | 0.027746 | 0.035469 | 0.045629 | 0.058992 | 0.069416 | 0.087012 | 0.11672 | 0.14702 | 0.18167 | 0.23092 | 0.28348 | 0.3471 | 0.41787 | 0.49639 | 0.57052 | 0.6315 | 0.66609 | 0.66868 | 0.64015 | 0.58783 | 0.52385 | 0.45806 | 0.3962 | 0.3406 | 0.2936 | 0.25428 | 0.22269 | 0.19622 | 0.17597 | 0.15804 | 0.14279 | 0.13021 | 0.12053 | 0.11142 | 0.10593 | 0.099251 | 0.10112 | 0.096409 | 0.099903 | 0.099379 | 0.11049 | 0.12227 | 0.13167 | 0.14829 | 0.16415 | 0.18118 | 0.20571 | 0.22768 | 0.25157 | 0.27443
Time 5.03 h, -20 celcius | 0.0046903 | 0.0060276 | 0.0048957 | 0.0052689 | 0.0080706 | 0.0070995 | 0.0085621 | 0.011385 | 0.014441 | 0.017939 | 0.023068 | 0.028754 | 0.036271 | 0.045614 | 0.058069 | 0.073874 | 0.094576 | 0.12111 | 0.15588 | 0.20027 | 0.2566 | 0.32289 | 0.39693 | 0.47149 | 0.53464 | 0.57592 | 0.58749 | 0.56901 | 0.52696 | 0.47094 | 0.40966 | 0.35018 | 0.29633 | 0.24993 | 0.21217 | 0.18272 | 0.16189 | 0.14492 | 0.13366 | 0.12856 | 0.12752 | 0.12988 | 0.13813 | 0.14441 | 0.16577 | 0.18416 | 0.20379 | 0.22754 | 0.25211 | 0.27626 | 0.29768
Time 8.5 h, -40 celcius | 0.0037257 | 0.0037257 | 0.0022099 | 0.0055149 | 0.0027352 | 0.0046061 | 0.0028107 | 0.0031095 | 0.0040131 | 0.0050574 | 0.0061923 | 0.007861 | 0.0096387 | 0.01196 | 0.014763 | 0.018394 | 0.022849 | 0.028488 | 0.035374 | 0.043956 | 0.054453 | 0.067485 | 0.083211 | 0.10248 | 0.12627 | 0.15518 | 0.19059 | 0.23316 | 0.28257 | 0.33712 | 0.39303 | 0.44437 | 0.48479 | 0.5087 | 0.51347 | 0.50011 | 0.47159 | 0.43276 | 0.38638 | 0.3379 | 0.29199 | 0.24717 | 0.21022 | 0.17522 | 0.14921 | 0.12645 | 0.10764 | 0.094062 | 0.085294 | 0.077832 | 0.076166 | 0.074374
Std. : Water (1:0)_ 5 g_17C | 0.40745 | 0.37758 | 0.33167 | 0.27797 | 0.22443 | 0.19417 | 0.16169 | 0.13849 | 0.12143 | 0.10697 | 0.096405 | 0.087034 | 0.081871 | 0.078656 | 0.076272 | 0.075226 | 0.07448 | 0.073601 | 0.073296 | 0.073701 | 0.074654 | 0.075483 | 0.075353 | 0.07631 | 0.0769 | 0.077719 | 0.079173 | 0.081297 | 0.084848 | 0.090883 | 0.098449 | 0.10715 | 0.11892 | 0.13057 | 0.14131 | 0.15224 | 0.161 | 0.1718 | 0.18315 | 0.19373 | 0.20789 | 0.22266 | 0.23803 | 0.25543 | 0.2743 | 0.29629 | 0.32039 | 0.34659
Std. : Water (1:3)_5 g_22.3C | 0.35022 | 0.37378 | 0.41173 | 0.55328 | 0.59494 | 0.61621 | 0.60526 | 0.57334 | 0.52449 | 0.45124 | 0.3927 | 0.33463 | 0.28521 | 0.24069 | 0.2067 | 0.17971 | 0.15895 | 0.14354 | 0.13098 | 0.1209 | 0.11373 | 0.10865 | 0.10508 | 0.10263 | 0.10025 | 0.099388 | 0.099009 | 0.09943 | 0.10029 | 0.10249 | 0.10653 | 0.11105 | 0.11816 | 0.12566 | 0.13766 | 0.14944 | 0.16023 | 0.17158 | 0.18231 | 0.19465 | 0.20803 | 0.22162 | 0.23412 | 0.25639 | 0.27568 | 0.29801 | 0.32242 | 0.35086 | 0.38221 | 0.41669
Fitting-Time 0.23 h (20.3 C) Liquid | 0.00080148 | 0.001009 | 0.0012703 | 0.0015992 | 0.0020132 | 0.0025345 | 0.0031908 | 0.0040169 | 0.005057 | 0.0063663 | 0.0080146 | 0.010089 | 0.012702 | 0.01599 | 0.020128 | 0.025337 | 0.031892 | 0.040136 | 0.050507 | 0.063538 | 0.07988 | 0.10037 | 0.126 | 0.15786 | 0.1972 | 0.24538 | 0.30315 | 0.37047 | 0.44655 | 0.52567 | 0.59992 | 0.65886 | 0.68897 | 0.68388 | 0.64493 | 0.58011 | 0.50283 | 0.42213 | 0.34988 | 0.28493 | 0.23165 | 0.18163 | 0.14738 | 0.11839 | 0.089082 | 0.071374 | 0.059526 | 0.041708 | 0.035758 | 0.029805 | 0.023848
Fitting-Time 5.03 h (-20 C) Frozen | 0.0048296 | 0.0060799 | 0.0076542 | 0.0096359 | 0.01213 | 0.01527 | 0.019222 | 0.024195 | 0.030452 | 0.038322 | 0.048213 | 0.060635 | 0.076215 | 0.095709 | 0.12001 | 0.15014 | 0.18717 | 0.232 | 0.28517 | 0.34602 | 0.41191 | 0.4775 | 0.53412 | 0.57135 | 0.58091 | 0.56037 | 0.51476 | 0.45386 | 0.38691 | 0.32252 | 0.26465 | 0.2141 | 0.17243 | 0.138 | 0.11029 | 0.087693 | 0.069745 | 0.055173 | 0.044035 | 0.034967 | 0.027983 | 0.021692 | 0.017495 | 0.013998 | 0.010499 | 0.0083994 | 0.0069995 | 0.0048997 | 0.0041998 | 0.0034999 | 0.0027999
(I)
18 GHz
20.3 °C
20.3 °C
18 kHz
0.0056 M KCl
(II)
0.0056 M KCl
TVIS range
Real part Capacitance
Imaginary part Capacitance
Measurement vial
+
-
-
+
+
+
+
+
+
+
+
+
+
+
-
-
-
-
-
-
-
-
-
-
+
+
+
+
+
+
+
+
+
+
-
-
-
-
-
-
-
-
-
-
Water
Glass wall
Electronic polarization
Atomic polarization
o
H
H
δ-
δ+
δ+
Dipolar polarization
Grotthus mechanism
o
H
H
δ-
δ+
δ+
o
H
H
δ-
δ+
δ+
H
o
H
H
o
H
H
o
H
H+
Ionic diffusion
H+
HCO3−
Na+
Cl−
H+
H+
OH-
H+
K+
K+
Cl−
Application: Determine leaching of ions
from the glass vial
pure
water
pure
water
Notes: As you can see here
from the addition of low levels of electrolyte (5.6 mM KCl)
That the characteristic frequency and the amplitude of the process are strongly dependent
on the conductivity of the liquid
One application might be to determine
the contamination of water from soluble components in the glass

## Slide 22: Dielectric Loss Mechanisms
The dielectric polarization of ice at −20 ˚C, with a dielectric loss peak frequencies of 2.57 kHz
Chart: Log Frequency
| 6 | 5.9030899869919438 | 5.8239109124113 | 5.7569630370485534 | 5.6020599913279625 | 5.5228744023138034 | 5.4259741609193757 | 5.3010299956639813 | 5.204119982655925 | 5.1106906972737542 | 5 | 4.9030899869919438 | 4.8027190075796815 | 4.7044336600521994 | 4.6020599913279625 | 4.5016890119157003 | 4.4006588497649739 | 4.3010299956639813 | 4.200659016251719 | 4.1009905230699646 | 4 | 3.90049275542937 | 3.800655228145212 | 3.7000543856282389 | 3.6003302305807652 | 3.5003188237463867 | 3.4001233554370809 | 3.3001605369513523 | 3.2001388538573807 | 3.1000257301078626 | 3 | 2.9000611027354806 | 2.8000362418279794 | 2.7000023971422538 | 2.6000249038929866 | 2.5000030680516931 | 2.4000023459279558 | 2.3000082025538129 | 2.2000018654066018 | 2.0999912335446846 | 2 | 1.9000009651534695 | 1.8000018278179688 | 1.700002397142254 | 1.6000030866277404 | 1.5000030680516931 | 1.400002345927956 | 1.3000082025538131 | 1.2000018654066018 | 1.0999912335446844 | 1
Time 0.23 h, 20.3 celcius | 1.0162 | 1.0162 | 1.0162 | 1.0162 | 1.0176 | 1.024 | 1.0293 | 1.0371 | 1.0465 | 1.0575 | 1.0742 | 1.0971 | 1.131 | 1.18 | 1.2538 | 1.3532 | 1.4803 | 1.6281 | 1.7827 | 1.9288 | 2.0567 | 2.1587 | 2.2374 | 2.2971 | 2.3414 | 2.3756 | 2.4038 | 2.4272 | 2.4476 | 2.4662 | 2.4852 | 2.5003 | 2.5152 | 2.5286 | 2.5419 | 2.5531 | 2.5615 | 2.5717 | 2.5802 | 2.589 | 2.5992 | 2.6061 | 2.6201 | 2.625 | 2.6478 | 2.6645 | 2.686 | 2.708 | 2.7359 | 2.7645 | 2.7969
Time 5.03 h, -20 celcius | 0.084287 | 0.084287 | 0.084287 | 0.084287 | 0.083003 | 0.084127 | 0.084469 | 0.085543 | 0.086743 | 0.087572 | 0.088047 | 0.088435 | 0.088561 | 0.088505 | 0.088289 | 0.08811 | 0.08822 | 0.08935 | 0.092855 | 0.10126 | 0.11875 | 0.15045 | 0.2025 | 0.28088 | 0.38519 | 0.51085 | 0.64628 | 0.77735 | 0.89303 | 0.98847 | 1.0619 | 1.1159 | 1.155 | 1.183 | 1.203 | 1.2167 | 1.2267 | 1.2373 | 1.2444 | 1.2521 | 1.2603 | 1.2702 | 1.2796 | 1.2944 | 1.3089 | 1.3285 | 1.3531 | 1.3812 | 1.4143 | 1.4539 | 1.499
Time 8.5 h, -40 celcius | 0.083695 | 0.083695 | 0.083695 | 0.083695 | 0.083695 | 0.08324 | 0.083622 | 0.083847 | 0.084834 | 0.086128 | 0.086714 | 0.087381 | 0.087886 | 0.088558 | 0.089009 | 0.089429 | 0.089952 | 0.090576 | 0.09152 | 0.092833 | 0.094685 | 0.097293 | 0.10083 | 0.10562 | 0.11226 | 0.12153 | 0.13502 | 0.15512 | 0.18502 | 0.22832 | 0.28819 | 0.36571 | 0.45912 | 0.56375 | 0.67242 | 0.77798 | 0.87404 | 0.95702 | 1.0284 | 1.0845 | 1.1268 | 1.1614 | 1.1873 | 1.2052 | 1.2167 | 1.2287 | 1.2359 | 1.2394 | 1.2468 | 1.2512 | 1.2552 | 1.2597
Std. : Water (1:0)_ 5 g_17C | 2.3304 | 2.4387 | 2.4947 | 2.5334 | 2.5734 | 2.595 | 2.6101 | 2.6237 | 2.6363 | 2.6458 | 2.6525 | 2.6605 | 2.6675 | 2.6754 | 2.6841 | 2.6936 | 2.7028 | 2.7121 | 2.7221 | 2.732 | 2.7416 | 2.7519 | 2.7627 | 2.773 | 2.7842 | 2.7949 | 2.8043 | 2.8148 | 2.8246 | 2.8354 | 2.8466 | 2.8598 | 2.8739 | 2.8899 | 2.908 | 2.9285 | 2.9493 | 2.972 | 2.9971 | 3.0212 | 3.0504 | 3.076 | 3.1069 | 3.1381 | 3.1714 | 3.2072 | 3.2459 | 3.2864
Std. : Water (1:3)_5 g_22.3C | 1.4671 | 1.6855 | 1.744 | 1.8824 | 1.9929 | 2.1292 | 2.3085 | 2.4363 | 2.5381 | 2.631 | 2.6959 | 2.7426 | 2.7767 | 2.8037 | 2.8219 | 2.8373 | 2.8512 | 2.8646 | 2.8761 | 2.8875 | 2.8997 | 2.9118 | 2.9235 | 2.9355 | 2.9478 | 2.9606 | 2.9734 | 2.9866 | 2.9991 | 3.0123 | 3.0249 | 3.039 | 3.0531 | 3.0685 | 3.0846 | 3.1036 | 3.1223 | 3.1442 | 3.1674 | 3.1919 | 3.2199 | 3.2461 | 3.2797 | 3.3073 | 3.3426 | 3.3775 | 3.4158 | 3.4569 | 3.5017 | 3.5489
Fitting-Time 0.23 h (20.3 C) Liquid | 2.412 | 2.412 | 2.412 | 2.412 | 2.412 | 2.412 | 2.412 | 2.412 | 2.412 | 2.4119 | 2.4119 | 2.4119 | 2.4119 | 2.4118 | 2.4117 | 2.4115 | 2.4112 | 2.4108 | 2.4101 | 2.409 | 2.4073 | 2.4046 | 2.4004 | 2.3937 | 2.3832 | 2.367 | 2.342 | 2.3043 | 2.2484 | 2.1697 | 2.0642 | 1.9301 | 1.7781 | 1.6192 | 1.4715 | 1.3445 | 1.2461 | 1.1731 | 1.1243 | 1.0907 | 1.0692 | 1.0535 | 1.0451 | 1.0395 | 1.035 | 1.0329 | 1.0318 | 1.0305 | 1.0302 | 1.0299 | 1.0297
Fitting-Time 5.03 h (-20 C) Frozen | 1.2389 | 1.2389 | 1.2389 | 1.2389 | 1.2388 | 1.2387 | 1.2386 | 1.2384 | 1.2381 | 1.2377 | 1.2369 | 1.2358 | 1.2339 | 1.231 | 1.2264 | 1.2192 | 1.208 | 1.1906 | 1.1642 | 1.1248 | 1.0679 | 0.98926 | 0.88724 | 0.76529 | 0.63274 | 0.50242 | 0.38716 | 0.29408 | 0.22349 | 0.17372 | 0.13979 | 0.11692 | 0.10222 | 0.092682 | 0.086624 | 0.08272 | 0.080267 | 0.078693 | 0.077739 | 0.077121 | 0.076743 | 0.076474 | 0.076332 | 0.076237 | 0.076164 | 0.07613 | 0.076111 | 0.076089 | 0.076084 | 0.076079 | 0.076076
Chart: Log Frequency
| 6 | 5.9030899869919438 | 5.8239109124113 | 5.7569630370485534 | 5.6020599913279625 | 5.5228744023138034 | 5.4259741609193757 | 5.3010299956639813 | 5.204119982655925 | 5.1106906972737542 | 5 | 4.9030899869919438 | 4.8027190075796815 | 4.7044336600521994 | 4.6020599913279625 | 4.5016890119157003 | 4.4006588497649739 | 4.3010299956639813 | 4.200659016251719 | 4.1009905230699646 | 4 | 3.90049275542937 | 3.800655228145212 | 3.7000543856282389 | 3.6003302305807652 | 3.5003188237463867 | 3.4001233554370809 | 3.3001605369513523 | 3.2001388538573807 | 3.1000257301078626 | 3 | 2.9000611027354806 | 2.8000362418279794 | 2.7000023971422538 | 2.6000249038929866 | 2.5000030680516931 | 2.4000023459279558 | 2.3000082025538129 | 2.2000018654066018 | 2.0999912335446846 | 2 | 1.9000009651534695 | 1.8000018278179688 | 1.700002397142254 | 1.6000030866277404 | 1.5000030680516931 | 1.400002345927956 | 1.3000082025538131 | 1.2000018654066018 | 1.0999912335446844 | 1
Time 0.23 h, 20.3 celcius | 0.021874 | 0.027746 | 0.035469 | 0.045629 | 0.058992 | 0.069416 | 0.087012 | 0.11672 | 0.14702 | 0.18167 | 0.23092 | 0.28348 | 0.3471 | 0.41787 | 0.49639 | 0.57052 | 0.6315 | 0.66609 | 0.66868 | 0.64015 | 0.58783 | 0.52385 | 0.45806 | 0.3962 | 0.3406 | 0.2936 | 0.25428 | 0.22269 | 0.19622 | 0.17597 | 0.15804 | 0.14279 | 0.13021 | 0.12053 | 0.11142 | 0.10593 | 0.099251 | 0.10112 | 0.096409 | 0.099903 | 0.099379 | 0.11049 | 0.12227 | 0.13167 | 0.14829 | 0.16415 | 0.18118 | 0.20571 | 0.22768 | 0.25157 | 0.27443
Time 5.03 h, -20 celcius | 0.0046903 | 0.0060276 | 0.0048957 | 0.0052689 | 0.0080706 | 0.0070995 | 0.0085621 | 0.011385 | 0.014441 | 0.017939 | 0.023068 | 0.028754 | 0.036271 | 0.045614 | 0.058069 | 0.073874 | 0.094576 | 0.12111 | 0.15588 | 0.20027 | 0.2566 | 0.32289 | 0.39693 | 0.47149 | 0.53464 | 0.57592 | 0.58749 | 0.56901 | 0.52696 | 0.47094 | 0.40966 | 0.35018 | 0.29633 | 0.24993 | 0.21217 | 0.18272 | 0.16189 | 0.14492 | 0.13366 | 0.12856 | 0.12752 | 0.12988 | 0.13813 | 0.14441 | 0.16577 | 0.18416 | 0.20379 | 0.22754 | 0.25211 | 0.27626 | 0.29768
Time 8.5 h, -40 celcius | 0.0037257 | 0.0037257 | 0.0022099 | 0.0055149 | 0.0027352 | 0.0046061 | 0.0028107 | 0.0031095 | 0.0040131 | 0.0050574 | 0.0061923 | 0.007861 | 0.0096387 | 0.01196 | 0.014763 | 0.018394 | 0.022849 | 0.028488 | 0.035374 | 0.043956 | 0.054453 | 0.067485 | 0.083211 | 0.10248 | 0.12627 | 0.15518 | 0.19059 | 0.23316 | 0.28257 | 0.33712 | 0.39303 | 0.44437 | 0.48479 | 0.5087 | 0.51347 | 0.50011 | 0.47159 | 0.43276 | 0.38638 | 0.3379 | 0.29199 | 0.24717 | 0.21022 | 0.17522 | 0.14921 | 0.12645 | 0.10764 | 0.094062 | 0.085294 | 0.077832 | 0.076166 | 0.074374
Std. : Water (1:0)_ 5 g_17C | 0.40745 | 0.37758 | 0.33167 | 0.27797 | 0.22443 | 0.19417 | 0.16169 | 0.13849 | 0.12143 | 0.10697 | 0.096405 | 0.087034 | 0.081871 | 0.078656 | 0.076272 | 0.075226 | 0.07448 | 0.073601 | 0.073296 | 0.073701 | 0.074654 | 0.075483 | 0.075353 | 0.07631 | 0.0769 | 0.077719 | 0.079173 | 0.081297 | 0.084848 | 0.090883 | 0.098449 | 0.10715 | 0.11892 | 0.13057 | 0.14131 | 0.15224 | 0.161 | 0.1718 | 0.18315 | 0.19373 | 0.20789 | 0.22266 | 0.23803 | 0.25543 | 0.2743 | 0.29629 | 0.32039 | 0.34659
Std. : Water (1:3)_5 g_22.3C | 0.35022 | 0.37378 | 0.41173 | 0.55328 | 0.59494 | 0.61621 | 0.60526 | 0.57334 | 0.52449 | 0.45124 | 0.3927 | 0.33463 | 0.28521 | 0.24069 | 0.2067 | 0.17971 | 0.15895 | 0.14354 | 0.13098 | 0.1209 | 0.11373 | 0.10865 | 0.10508 | 0.10263 | 0.10025 | 0.099388 | 0.099009 | 0.09943 | 0.10029 | 0.10249 | 0.10653 | 0.11105 | 0.11816 | 0.12566 | 0.13766 | 0.14944 | 0.16023 | 0.17158 | 0.18231 | 0.19465 | 0.20803 | 0.22162 | 0.23412 | 0.25639 | 0.27568 | 0.29801 | 0.32242 | 0.35086 | 0.38221 | 0.41669
Fitting-Time 0.23 h (20.3 C) Liquid | 0.00080148 | 0.001009 | 0.0012703 | 0.0015992 | 0.0020132 | 0.0025345 | 0.0031908 | 0.0040169 | 0.005057 | 0.0063663 | 0.0080146 | 0.010089 | 0.012702 | 0.01599 | 0.020128 | 0.025337 | 0.031892 | 0.040136 | 0.050507 | 0.063538 | 0.07988 | 0.10037 | 0.126 | 0.15786 | 0.1972 | 0.24538 | 0.30315 | 0.37047 | 0.44655 | 0.52567 | 0.59992 | 0.65886 | 0.68897 | 0.68388 | 0.64493 | 0.58011 | 0.50283 | 0.42213 | 0.34988 | 0.28493 | 0.23165 | 0.18163 | 0.14738 | 0.11839 | 0.089082 | 0.071374 | 0.059526 | 0.041708 | 0.035758 | 0.029805 | 0.023848
Fitting-Time 5.03 h (-20 C) Frozen | 0.0048296 | 0.0060799 | 0.0076542 | 0.0096359 | 0.01213 | 0.01527 | 0.019222 | 0.024195 | 0.030452 | 0.038322 | 0.048213 | 0.060635 | 0.076215 | 0.095709 | 0.12001 | 0.15014 | 0.18717 | 0.232 | 0.28517 | 0.34602 | 0.41191 | 0.4775 | 0.53412 | 0.57135 | 0.58091 | 0.56037 | 0.51476 | 0.45386 | 0.38691 | 0.32252 | 0.26465 | 0.2141 | 0.17243 | 0.138 | 0.11029 | 0.087693 | 0.069745 | 0.055173 | 0.044035 | 0.034967 | 0.027983 | 0.021692 | 0.017495 | 0.013998 | 0.010499 | 0.0083994 | 0.0069995 | 0.0048997 | 0.0041998 | 0.0034999 | 0.0027999
(I)
18 GHz
20.3 °C
20.3 °C
18 kHz
0.0056 M KCl
0.0056 M KCl
(II)
-20 °C
(III)
2.6 kHz
-20 °C
Real part Capacitance
Imaginary part Capacitance
Measurement vial
Co
+
-
-
+
+
+
+
+
+
+
+
+
+
+
-
-
-
-
-
-
-
-
-
-
+
+
+
+
+
+
+
+
+
+
-
-
-
-
-
-
-
-
-
-
Ice
Glass wall
Electronic polarization
Atomic polarization
L- and D- orientation defects
Application: Ice mass
Notes: The next one is particularly interesting because it relates to the formation and properties of the ice fraction
There are a number of applications for this process
The first is the determination of the amount of ice that forms

## Slide 23: Dielectric Loss Mechanisms
The dielectric polarization of ice at −40 ˚C with a dielectric loss peak frequencies of 537 Hz.
Chart: Log Frequency
| 6 | 5.9030899869919438 | 5.8239109124113 | 5.7569630370485534 | 5.6020599913279625 | 5.5228744023138034 | 5.4259741609193757 | 5.3010299956639813 | 5.204119982655925 | 5.1106906972737542 | 5 | 4.9030899869919438 | 4.8027190075796815 | 4.7044336600521994 | 4.6020599913279625 | 4.5016890119157003 | 4.4006588497649739 | 4.3010299956639813 | 4.200659016251719 | 4.1009905230699646 | 4 | 3.90049275542937 | 3.800655228145212 | 3.7000543856282389 | 3.6003302305807652 | 3.5003188237463867 | 3.4001233554370809 | 3.3001605369513523 | 3.2001388538573807 | 3.1000257301078626 | 3 | 2.9000611027354806 | 2.8000362418279794 | 2.7000023971422538 | 2.6000249038929866 | 2.5000030680516931 | 2.4000023459279558 | 2.3000082025538129 | 2.2000018654066018 | 2.0999912335446846 | 2 | 1.9000009651534695 | 1.8000018278179688 | 1.700002397142254 | 1.6000030866277404 | 1.5000030680516931 | 1.400002345927956 | 1.3000082025538131 | 1.2000018654066018 | 1.0999912335446844 | 1
Time 0.23 h, 20.3 celcius | 1.0162 | 1.0162 | 1.0162 | 1.0162 | 1.0176 | 1.024 | 1.0293 | 1.0371 | 1.0465 | 1.0575 | 1.0742 | 1.0971 | 1.131 | 1.18 | 1.2538 | 1.3532 | 1.4803 | 1.6281 | 1.7827 | 1.9288 | 2.0567 | 2.1587 | 2.2374 | 2.2971 | 2.3414 | 2.3756 | 2.4038 | 2.4272 | 2.4476 | 2.4662 | 2.4852 | 2.5003 | 2.5152 | 2.5286 | 2.5419 | 2.5531 | 2.5615 | 2.5717 | 2.5802 | 2.589 | 2.5992 | 2.6061 | 2.6201 | 2.625 | 2.6478 | 2.6645 | 2.686 | 2.708 | 2.7359 | 2.7645 | 2.7969
Time 5.03 h, -20 celcius | 0.084287 | 0.084287 | 0.084287 | 0.084287 | 0.083003 | 0.084127 | 0.084469 | 0.085543 | 0.086743 | 0.087572 | 0.088047 | 0.088435 | 0.088561 | 0.088505 | 0.088289 | 0.08811 | 0.08822 | 0.08935 | 0.092855 | 0.10126 | 0.11875 | 0.15045 | 0.2025 | 0.28088 | 0.38519 | 0.51085 | 0.64628 | 0.77735 | 0.89303 | 0.98847 | 1.0619 | 1.1159 | 1.155 | 1.183 | 1.203 | 1.2167 | 1.2267 | 1.2373 | 1.2444 | 1.2521 | 1.2603 | 1.2702 | 1.2796 | 1.2944 | 1.3089 | 1.3285 | 1.3531 | 1.3812 | 1.4143 | 1.4539 | 1.499
Time 8.5 h, -40 celcius | 0.083695 | 0.083695 | 0.083695 | 0.083695 | 0.083695 | 0.08324 | 0.083622 | 0.083847 | 0.084834 | 0.086128 | 0.086714 | 0.087381 | 0.087886 | 0.088558 | 0.089009 | 0.089429 | 0.089952 | 0.090576 | 0.09152 | 0.092833 | 0.094685 | 0.097293 | 0.10083 | 0.10562 | 0.11226 | 0.12153 | 0.13502 | 0.15512 | 0.18502 | 0.22832 | 0.28819 | 0.36571 | 0.45912 | 0.56375 | 0.67242 | 0.77798 | 0.87404 | 0.95702 | 1.0284 | 1.0845 | 1.1268 | 1.1614 | 1.1873 | 1.2052 | 1.2167 | 1.2287 | 1.2359 | 1.2394 | 1.2468 | 1.2512 | 1.2552 | 1.2597
Std. : Water (1:0)_ 5 g_17C | 2.3304 | 2.4387 | 2.4947 | 2.5334 | 2.5734 | 2.595 | 2.6101 | 2.6237 | 2.6363 | 2.6458 | 2.6525 | 2.6605 | 2.6675 | 2.6754 | 2.6841 | 2.6936 | 2.7028 | 2.7121 | 2.7221 | 2.732 | 2.7416 | 2.7519 | 2.7627 | 2.773 | 2.7842 | 2.7949 | 2.8043 | 2.8148 | 2.8246 | 2.8354 | 2.8466 | 2.8598 | 2.8739 | 2.8899 | 2.908 | 2.9285 | 2.9493 | 2.972 | 2.9971 | 3.0212 | 3.0504 | 3.076 | 3.1069 | 3.1381 | 3.1714 | 3.2072 | 3.2459 | 3.2864
Std. : Water (1:3)_5 g_22.3C | 1.4671 | 1.6855 | 1.744 | 1.8824 | 1.9929 | 2.1292 | 2.3085 | 2.4363 | 2.5381 | 2.631 | 2.6959 | 2.7426 | 2.7767 | 2.8037 | 2.8219 | 2.8373 | 2.8512 | 2.8646 | 2.8761 | 2.8875 | 2.8997 | 2.9118 | 2.9235 | 2.9355 | 2.9478 | 2.9606 | 2.9734 | 2.9866 | 2.9991 | 3.0123 | 3.0249 | 3.039 | 3.0531 | 3.0685 | 3.0846 | 3.1036 | 3.1223 | 3.1442 | 3.1674 | 3.1919 | 3.2199 | 3.2461 | 3.2797 | 3.3073 | 3.3426 | 3.3775 | 3.4158 | 3.4569 | 3.5017 | 3.5489
Fitting-Time 0.23 h (20.3 C) Liquid | 2.412 | 2.412 | 2.412 | 2.412 | 2.412 | 2.412 | 2.412 | 2.412 | 2.412 | 2.4119 | 2.4119 | 2.4119 | 2.4119 | 2.4118 | 2.4117 | 2.4115 | 2.4112 | 2.4108 | 2.4101 | 2.409 | 2.4073 | 2.4046 | 2.4004 | 2.3937 | 2.3832 | 2.367 | 2.342 | 2.3043 | 2.2484 | 2.1697 | 2.0642 | 1.9301 | 1.7781 | 1.6192 | 1.4715 | 1.3445 | 1.2461 | 1.1731 | 1.1243 | 1.0907 | 1.0692 | 1.0535 | 1.0451 | 1.0395 | 1.035 | 1.0329 | 1.0318 | 1.0305 | 1.0302 | 1.0299 | 1.0297
Fitting-Time 5.03 h (-20 C) Frozen | 1.2389 | 1.2389 | 1.2389 | 1.2389 | 1.2388 | 1.2387 | 1.2386 | 1.2384 | 1.2381 | 1.2377 | 1.2369 | 1.2358 | 1.2339 | 1.231 | 1.2264 | 1.2192 | 1.208 | 1.1906 | 1.1642 | 1.1248 | 1.0679 | 0.98926 | 0.88724 | 0.76529 | 0.63274 | 0.50242 | 0.38716 | 0.29408 | 0.22349 | 0.17372 | 0.13979 | 0.11692 | 0.10222 | 0.092682 | 0.086624 | 0.08272 | 0.080267 | 0.078693 | 0.077739 | 0.077121 | 0.076743 | 0.076474 | 0.076332 | 0.076237 | 0.076164 | 0.07613 | 0.076111 | 0.076089 | 0.076084 | 0.076079 | 0.076076
Chart: Log Frequency
| 6 | 5.9030899869919438 | 5.8239109124113 | 5.7569630370485534 | 5.6020599913279625 | 5.5228744023138034 | 5.4259741609193757 | 5.3010299956639813 | 5.204119982655925 | 5.1106906972737542 | 5 | 4.9030899869919438 | 4.8027190075796815 | 4.7044336600521994 | 4.6020599913279625 | 4.5016890119157003 | 4.4006588497649739 | 4.3010299956639813 | 4.200659016251719 | 4.1009905230699646 | 4 | 3.90049275542937 | 3.800655228145212 | 3.7000543856282389 | 3.6003302305807652 | 3.5003188237463867 | 3.4001233554370809 | 3.3001605369513523 | 3.2001388538573807 | 3.1000257301078626 | 3 | 2.9000611027354806 | 2.8000362418279794 | 2.7000023971422538 | 2.6000249038929866 | 2.5000030680516931 | 2.4000023459279558 | 2.3000082025538129 | 2.2000018654066018 | 2.0999912335446846 | 2 | 1.9000009651534695 | 1.8000018278179688 | 1.700002397142254 | 1.6000030866277404 | 1.5000030680516931 | 1.400002345927956 | 1.3000082025538131 | 1.2000018654066018 | 1.0999912335446844 | 1
Time 0.23 h, 20.3 celcius | 0.021874 | 0.027746 | 0.035469 | 0.045629 | 0.058992 | 0.069416 | 0.087012 | 0.11672 | 0.14702 | 0.18167 | 0.23092 | 0.28348 | 0.3471 | 0.41787 | 0.49639 | 0.57052 | 0.6315 | 0.66609 | 0.66868 | 0.64015 | 0.58783 | 0.52385 | 0.45806 | 0.3962 | 0.3406 | 0.2936 | 0.25428 | 0.22269 | 0.19622 | 0.17597 | 0.15804 | 0.14279 | 0.13021 | 0.12053 | 0.11142 | 0.10593 | 0.099251 | 0.10112 | 0.096409 | 0.099903 | 0.099379 | 0.11049 | 0.12227 | 0.13167 | 0.14829 | 0.16415 | 0.18118 | 0.20571 | 0.22768 | 0.25157 | 0.27443
Time 5.03 h, -20 celcius | 0.0046903 | 0.0060276 | 0.0048957 | 0.0052689 | 0.0080706 | 0.0070995 | 0.0085621 | 0.011385 | 0.014441 | 0.017939 | 0.023068 | 0.028754 | 0.036271 | 0.045614 | 0.058069 | 0.073874 | 0.094576 | 0.12111 | 0.15588 | 0.20027 | 0.2566 | 0.32289 | 0.39693 | 0.47149 | 0.53464 | 0.57592 | 0.58749 | 0.56901 | 0.52696 | 0.47094 | 0.40966 | 0.35018 | 0.29633 | 0.24993 | 0.21217 | 0.18272 | 0.16189 | 0.14492 | 0.13366 | 0.12856 | 0.12752 | 0.12988 | 0.13813 | 0.14441 | 0.16577 | 0.18416 | 0.20379 | 0.22754 | 0.25211 | 0.27626 | 0.29768
Time 8.5 h, -40 celcius | 0.0037257 | 0.0037257 | 0.0022099 | 0.0055149 | 0.0027352 | 0.0046061 | 0.0028107 | 0.0031095 | 0.0040131 | 0.0050574 | 0.0061923 | 0.007861 | 0.0096387 | 0.01196 | 0.014763 | 0.018394 | 0.022849 | 0.028488 | 0.035374 | 0.043956 | 0.054453 | 0.067485 | 0.083211 | 0.10248 | 0.12627 | 0.15518 | 0.19059 | 0.23316 | 0.28257 | 0.33712 | 0.39303 | 0.44437 | 0.48479 | 0.5087 | 0.51347 | 0.50011 | 0.47159 | 0.43276 | 0.38638 | 0.3379 | 0.29199 | 0.24717 | 0.21022 | 0.17522 | 0.14921 | 0.12645 | 0.10764 | 0.094062 | 0.085294 | 0.077832 | 0.076166 | 0.074374
Std. : Water (1:0)_ 5 g_17C | 0.40745 | 0.37758 | 0.33167 | 0.27797 | 0.22443 | 0.19417 | 0.16169 | 0.13849 | 0.12143 | 0.10697 | 0.096405 | 0.087034 | 0.081871 | 0.078656 | 0.076272 | 0.075226 | 0.07448 | 0.073601 | 0.073296 | 0.073701 | 0.074654 | 0.075483 | 0.075353 | 0.07631 | 0.0769 | 0.077719 | 0.079173 | 0.081297 | 0.084848 | 0.090883 | 0.098449 | 0.10715 | 0.11892 | 0.13057 | 0.14131 | 0.15224 | 0.161 | 0.1718 | 0.18315 | 0.19373 | 0.20789 | 0.22266 | 0.23803 | 0.25543 | 0.2743 | 0.29629 | 0.32039 | 0.34659
Std. : Water (1:3)_5 g_22.3C | 0.35022 | 0.37378 | 0.41173 | 0.55328 | 0.59494 | 0.61621 | 0.60526 | 0.57334 | 0.52449 | 0.45124 | 0.3927 | 0.33463 | 0.28521 | 0.24069 | 0.2067 | 0.17971 | 0.15895 | 0.14354 | 0.13098 | 0.1209 | 0.11373 | 0.10865 | 0.10508 | 0.10263 | 0.10025 | 0.099388 | 0.099009 | 0.09943 | 0.10029 | 0.10249 | 0.10653 | 0.11105 | 0.11816 | 0.12566 | 0.13766 | 0.14944 | 0.16023 | 0.17158 | 0.18231 | 0.19465 | 0.20803 | 0.22162 | 0.23412 | 0.25639 | 0.27568 | 0.29801 | 0.32242 | 0.35086 | 0.38221 | 0.41669
Fitting-Time 0.23 h (20.3 C) Liquid | 0.00080148 | 0.001009 | 0.0012703 | 0.0015992 | 0.0020132 | 0.0025345 | 0.0031908 | 0.0040169 | 0.005057 | 0.0063663 | 0.0080146 | 0.010089 | 0.012702 | 0.01599 | 0.020128 | 0.025337 | 0.031892 | 0.040136 | 0.050507 | 0.063538 | 0.07988 | 0.10037 | 0.126 | 0.15786 | 0.1972 | 0.24538 | 0.30315 | 0.37047 | 0.44655 | 0.52567 | 0.59992 | 0.65886 | 0.68897 | 0.68388 | 0.64493 | 0.58011 | 0.50283 | 0.42213 | 0.34988 | 0.28493 | 0.23165 | 0.18163 | 0.14738 | 0.11839 | 0.089082 | 0.071374 | 0.059526 | 0.041708 | 0.035758 | 0.029805 | 0.023848
Fitting-Time 5.03 h (-20 C) Frozen | 0.0048296 | 0.0060799 | 0.0076542 | 0.0096359 | 0.01213 | 0.01527 | 0.019222 | 0.024195 | 0.030452 | 0.038322 | 0.048213 | 0.060635 | 0.076215 | 0.095709 | 0.12001 | 0.15014 | 0.18717 | 0.232 | 0.28517 | 0.34602 | 0.41191 | 0.4775 | 0.53412 | 0.57135 | 0.58091 | 0.56037 | 0.51476 | 0.45386 | 0.38691 | 0.32252 | 0.26465 | 0.2141 | 0.17243 | 0.138 | 0.11029 | 0.087693 | 0.069745 | 0.055173 | 0.044035 | 0.034967 | 0.027983 | 0.021692 | 0.017495 | 0.013998 | 0.010499 | 0.0083994 | 0.0069995 | 0.0048997 | 0.0041998 | 0.0034999 | 0.0027999
(I)
18 GHz
20.3 °C
20.3 °C
18 kHz
(II)
-20 °C
2.6 kHz
-20 °C
-40 °C
-40 °C
537 Hz
(IV)
0.0056 M KCl
0.0056 M KCl
(III)
Real part Capacitance
Imaginary part Capacitance
Measurement vial
Co
+
-
-
+
+
+
+
+
+
+
+
+
+
+
-
-
-
-
-
-
-
-
-
-
+
+
+
+
+
+
+
+
+
+
-
-
-
-
-
-
-
-
-
-
Ice
Glass wall
Electronic polarization
Atomic polarization
Ionic defects
(similar to Grotthus mechanism)
Application: average ice temperature
Notes: You can see from this temperature change from -20 degC to to -40 degC
That the relaxation frequency of the dielectric loss peak [click]
Has a strong temperature dependence [click]
With a shift of one order of magnitude with a 20 deg C change in ice temperature [click]
Which can be exploited as a method for the non-invasive determination of the average ice temperature [click]

## Slide 24: Dielectric Loss Mechanisms
Application: high frequency real part
Capacitance for ice growth end point
Chart: Log Frequency
| 6 | 5.9030899869919438 | 5.8239109124113 | 5.7569630370485534 | 5.6020599913279625 | 5.5228744023138034 | 5.4259741609193757 | 5.3010299956639813 | 5.204119982655925 | 5.1106906972737542 | 5 | 4.9030899869919438 | 4.8027190075796815 | 4.7044336600521994 | 4.6020599913279625 | 4.5016890119157003 | 4.4006588497649739 | 4.3010299956639813 | 4.200659016251719 | 4.1009905230699646 | 4 | 3.90049275542937 | 3.800655228145212 | 3.7000543856282389 | 3.6003302305807652 | 3.5003188237463867 | 3.4001233554370809 | 3.3001605369513523 | 3.2001388538573807 | 3.1000257301078626 | 3 | 2.9000611027354806 | 2.8000362418279794 | 2.7000023971422538 | 2.6000249038929866 | 2.5000030680516931 | 2.4000023459279558 | 2.3000082025538129 | 2.2000018654066018 | 2.0999912335446846 | 2 | 1.9000009651534695 | 1.8000018278179688 | 1.700002397142254 | 1.6000030866277404 | 1.5000030680516931 | 1.400002345927956 | 1.3000082025538131 | 1.2000018654066018 | 1.0999912335446844 | 1
Time 0.23 h, 20.3 celcius | 1.0162 | 1.0162 | 1.0162 | 1.0162 | 1.0176 | 1.024 | 1.0293 | 1.0371 | 1.0465 | 1.0575 | 1.0742 | 1.0971 | 1.131 | 1.18 | 1.2538 | 1.3532 | 1.4803 | 1.6281 | 1.7827 | 1.9288 | 2.0567 | 2.1587 | 2.2374 | 2.2971 | 2.3414 | 2.3756 | 2.4038 | 2.4272 | 2.4476 | 2.4662 | 2.4852 | 2.5003 | 2.5152 | 2.5286 | 2.5419 | 2.5531 | 2.5615 | 2.5717 | 2.5802 | 2.589 | 2.5992 | 2.6061 | 2.6201 | 2.625 | 2.6478 | 2.6645 | 2.686 | 2.708 | 2.7359 | 2.7645 | 2.7969
Time 5.03 h, -20 celcius | 0.084287 | 0.084287 | 0.084287 | 0.084287 | 0.083003 | 0.084127 | 0.084469 | 0.085543 | 0.086743 | 0.087572 | 0.088047 | 0.088435 | 0.088561 | 0.088505 | 0.088289 | 0.08811 | 0.08822 | 0.08935 | 0.092855 | 0.10126 | 0.11875 | 0.15045 | 0.2025 | 0.28088 | 0.38519 | 0.51085 | 0.64628 | 0.77735 | 0.89303 | 0.98847 | 1.0619 | 1.1159 | 1.155 | 1.183 | 1.203 | 1.2167 | 1.2267 | 1.2373 | 1.2444 | 1.2521 | 1.2603 | 1.2702 | 1.2796 | 1.2944 | 1.3089 | 1.3285 | 1.3531 | 1.3812 | 1.4143 | 1.4539 | 1.499
Time 8.5 h, -40 celcius | 0.083695 | 0.083695 | 0.083695 | 0.083695 | 0.083695 | 0.08324 | 0.083622 | 0.083847 | 0.084834 | 0.086128 | 0.086714 | 0.087381 | 0.087886 | 0.088558 | 0.089009 | 0.089429 | 0.089952 | 0.090576 | 0.09152 | 0.092833 | 0.094685 | 0.097293 | 0.10083 | 0.10562 | 0.11226 | 0.12153 | 0.13502 | 0.15512 | 0.18502 | 0.22832 | 0.28819 | 0.36571 | 0.45912 | 0.56375 | 0.67242 | 0.77798 | 0.87404 | 0.95702 | 1.0284 | 1.0845 | 1.1268 | 1.1614 | 1.1873 | 1.2052 | 1.2167 | 1.2287 | 1.2359 | 1.2394 | 1.2468 | 1.2512 | 1.2552 | 1.2597
100 kHz
temperature
independent
10 Hz
temperature
dependent
Notes: Now if we focus on the real part capacitance and review the changes
as we transition [click] from liquid state at +20 C to the frozen state at -20 and – 40 degrees C
You can see that the capacitance of the ice changes with temperature at low frequency [click]
But is largely independent of temperature at high frequency [click]
Which can be exploited as a method for [click]
the determination of the ice growth end point

## Slide 25: TVIS publications suggestive of Z-FDM applications
Smith, G. & Jeeraruangrattana, Y. 2019, "Chapter 5 Through-Vial Impedance Spectroscopy (TVIS): A New Method for Determining the Ice Nucleation Temperature and the Solidification End Point " in Freeze Drying of Pharmaceutical Products, eds. D. Fissore, R. Pisano & A. Barresi, 1st edn, CRC Press, Florida, United States
Jeeraruangrattana, Y., Smith, G., Polygalov, E. and Ermolina, I. (2020) Determination of ice interface temperature, sublimation rate and the dried product resistance, and its application in the assessment of microcollapse using through-vial impedance spectroscopy. European Journal of Pharmaceutics and Biopharmaceutics, 152, pp. 144-163
Smith, G., Jeeraruangrattana, Y., Ermolina, I. (2018). The application of dual-electrode through vial impedance spectroscopy for the determination of ice interface temperatures, primary drying rate and vial heat transfer coefficient in lyophilization process development. European Journal of Pharmaceutics and Biopharmaceutics
Smith, G., Arshad, M.S., Polygalov, E., Ermolina, I., McCoy, T.R., Matejtschuk, P. (2017). Process Understanding in Freeze-Drying Cycle Development: Applications for Through-Vial Impedance Spectroscopy (TVIS) in Mini-pilot Studies. Journal of Pharmaceutical Innovation, 12 (1), pp. 26-40 Key observation was the potential to measure temperature non-invasively
Arshad, M.S., Smith, G., Polygalov, E., Ermolina, I. (2014). Through-vial impedance spectroscopy of critical events during the freezing stage of the lyophilization cycle: The example of the impact of sucrose on the crystallization of mannitol. European Journal of Pharmaceutics and Biopharmaceutics, 87 (3), pp. 598-605
Smith, G., Arshad, M.S., Polygalov, E., Ermolina, I. (2014). Through-Vial Impedance Spectroscopy of the Mechanisms of Annealing in the Freeze-Drying of Maltodextrin: The Impact of Annealing Hold Time and Temperature on the Primary Drying Rate. Journal of Pharmaceutical Sciences, 103 (6), pp. 1799-1810
Smith, G., Arshad, M.S., Polygalov, E. and Ermolina, I. (2013) An application for impedance spectroscopy in the characterisation of the glass transition during the lyophilization cycle: The example of a 10% w/v maltodextrin solution. European Journal of Pharmaceutics and Biopharmaceutics, 86 (3 Part B), pp. 1130-1140.
Nucleation Temperature and the Solidification End Point
Notes: I said that most of the work we have done to date
relates to the use of TVIS in the determination of various process parameters
(click) One of our most recent profiles the application I just mentioned
i.e. the use of TVIS in the non-invasive determination of nucleation temperature and solidification end point

## Slide 26: Dielectric relaxation of ice
5 mL water in
10 mL glass TVIS vial
(1 pair of 10/19 mm height/width electrodes)
2 µL water over IDE
(90 pairs of gold interdigitated electrodes)
10/10 m electrode width/spacing
1.6 kHz temperature sensitive
Notes: So it was based on these TVIS applications
that we started to look at applications for inter-digitated electrodes inside a freeze-drying microscope
You can see from the dielectric loss peak for ice that both systems display similar
but not exactly the same characteristics [CLICK]
And we can put this down to the influence of the glass wall on the TVIS measurement
[click] I have highlighted here the frequency of 1.6 kHz
Because that is the frequency I am going to focus on
In my studies freeze-drying microscope

## Slide 27
Observations on Sample Size
Case study of 5% w/v Sucrose Solution
Applications in freezing (nucleation temperature, ice growth rates, solidification end point)
Notes: The first relates to ice nucleation, growth and end point

## Slide 28
Nucleation of 0.5µL of 5% Sucrose
Notes: The top two graphs show the real and imaginary capacitance at the measurement frequency of 1.6 kHz
Whereas the bottom graph shows the temperature of the FDM stage
The temperature profile of the stage looks a bit odd
– at first appearing to increase [click] before then decreasing [click]
but this is typical of the temperature control of the stage
which undulates to some degree as the temperature is ramped.

## Slide 29: Nucleation of 0.5µL of 5% Sucrose
A. Nucleation
Temperature/time
B. Ice solidification
end point time/temp
Notes: The first point of interest is ice nucleation
[click] at time-line A
This point is shown by
[click] an inflection in the real part capacitance
[click] and an inflection in the imaginary capacitance [click]
The second point of interest is the ice solidification end point
[click] at time-line B
However, this only shown by
[click] an inflection in the real part capacitance.
[click] The imaginary capacitance continues to change through this point
because it is much more sensitive to the change in the temperature of the sample [click]

## Slide 30: Nucleation of 0.5µL of 5% Sucrose
A. Nucleation
Temperature/time
B. Ice solidification
end point time/temp
Time difference between time points A and B is the ice solidification time and hence provides an opportunity to measure ice growth rates at the mean ice growth temperature (C)
Ice solidification
time = 1.2 s
C. Mean ice growth
Temperature – 17.9
Notes: and so if we know the start of ice formation [click]
and end of ice formation [click]
we can work out the ice growth rates [click]

## Slide 31: Nucleation of 0.5µL of 5% Sucrose
3
2
6
5
4
1
1
2
3
4
5
6
A. Nucleation
Temperature/time
B. Ice solidification
end point time/temp
Notes: In contrast we don’t always see the same transitions in the images of the FDM microscope
Because they happen off screen so to speak
[click] This first image was acquired after the nucleation point A but doesn’t show any evidence of ice formation
[click] Its only when we record the next image that we see evidence of ice formation
[click] And in the third image shows the ice moving across the screen
[click] then by the time the 4th image is recorded the ice front has moved out of view
But the impedance data for image 5 shows that the process has not yet completed until image 6 is aquired

## Slide 32: Ice growth rates
Assumption: unfrozen fraction comprises 80:20 ratio of sucrose to water
1 mL of 5% w/w sucrose has 0.95 g water
It follows that 0.0125 g (0.05 x 20/80) is bound and produces 0.9375 g ice
Estimated from:
0.5 µL of 5% sucrose (produces 4.688E-04 g ice)
Ice formation time = 1.2 s (12 data points)
Ice growth rate: 4.688E-04 / 1.2 = 0.39 mg/s
Relevance in formation design :
ice crystal size? Dry layer resistance Rp and drying rates
Notes: With some simple calculations
based on assumptions concerning how much ice would form from the solution
(and the ice formation time from Z-FDM)
(click) We can calculate average growth rates
Here an average growth rate of 0.39 mg/s is recorded
[click] If we accept relative measurements of growth rates as a function of product formulation
Then it might give some indication of relative differences in ice crystal sizes,
and hence dry layer resistances and associated drying rates of different formulations

## Slide 33: Dielectric loss or dielectric permittivity analysis?
Freeze drying of 5% sucrose (0.05μL)
Studied by Image analysis
Applications in primary drying (drying rate, product collapse)
Notes: The next slides explore the application of Z-FDM in primary drying
But first we need to start with some work with did with image analysis

## Slide 34: FDM protocol
Time period for image analysis by Matlab
NB: Temperature and pressure measured on FDM every 100 ms
FDM freeze-drying of 5% sucrose solution (0.05 μL)
set temperature for the FDM stage
Liquid state
A
ice growth
B
ice solidification
C
sublimation
D
end of primary drying
E
Notes: The profile shown here is the set temperature for the FDM stage.
[click] Initially (at point A) the sample is in the liquid state
[click] as the temperature of the sample is reduced then we reach point B when ice appears in the image
[click] and almost immediately afterwards you reach the solidification end point (point C)
[click] after the vacuum is applied there is a loss of ice (as shown by a darkening around the perimeter of the image) – point D
[click] before reaching the end point E when all the ice has been removed.

## Slide 35: MATLAB® Image analysis (pixel counting)
Global templet generation – dried product image
Threshold test image – frozen image or drying stage image
Global pixel : 527515
MATLAB®
Dried product image
Product during drying
MATLAB®
Pixel for central area: 86317
FDM primary-drying of 5% sucrose soln (0.05 μL) at -35˚C
Notes: The next stage was to apply image analysis using a code written in MatLab
In the first step, we counted the dark pixels associated with the dried solution
And then we counted backwards to determine the ice layer from the white pixel count

## Slide 36: Pixel analysis
NB: Temperature and pressure measured every 100 ms
A: Application of vacuum
vacuum applied
vacuum stabilises
Notes: On the left scale you have the pixel count and the corresponding data (coloured in red, then yellow, then blue and finally green)
The red data shows the constant pixel count owing to the fact that drying hasn’t started
(click) Then immediately after the vacuum is applied there is an initial fast rate of drying (shown by the yellow line)
[click] which then slows down as the vacuum bottoms out to its set value
At that point and thereafter there is an almost linear decrease in ice mass
(which can be modelled satisfactorily by a second order polynomial)

## Slide 37: Drying rate determination
76µm
0.8 mm
0.62 mm
Area of perimeter
0.00342 cm2
NB: Sample thickness assumed from the Lactose sample analysed in the same setup.
Weight fraction of sucrose | 0.05 | (5% Sucrose)
Weight fraction of water | 0.95 | i.e. 95 % water
Weight fraction of bound water (1) | 0.0125 | 
Weight fraction of freezable water | 0.9375 | 
Sample volume | 0.05 | µL
Freezable water | 0.0469 | µL
Freezable water in mg | 0.0469 | mg of ice
Total pix before drying starts | 466873 | 
1 pixel (a) | 1.004E-07 | mg of ice
Gradient of linear part (b) | 132110 | pixel per min (yellow line)
Drying rate (a x b) | 0.0133 | mg min−1
Drying rate (B) | 0.00080 | g h−1
Area of perimeter of sample (A) | 0.00342 | cm2
Specific drying rate (B/A) | 0.233 | g h−1 cm−2
(1) based on 80:20 ratio of sugar to water in freeze-concentrated solution
Example drying rate from a 10 mL glass tubing vial is 0.25 g h-1
Vial diameter : 22 mm Internal area : 3.8 cm-1
Specific drying rate : 0.065 g h−1 cm−2
Difference due to differences in heat transfer etc.
Notes: With a few more calculations (again with some assumptions) we can arrive at an estimate for the specific drying rate.
Which in this case turns out to be 0.233 g per hour per cm2
This drying rate is must faster than the specific drying rate of 0.065 g per hour per cm2
that is observed in a glass vial
These differences are a consequence of differences in heat transfer etc.

## Slide 38: Drying rate at different gradient
NB: Temperature and pressure measured every 100 ms
Application of vacuum
B
C
B
B
Drying Rates
At A Initial – 0.00080g h-1
At B: Middle – 0.00050 g h-1
At C: Middle – 0.00041 g h-1
A
B
C
Notes: From the polynomial fit we can then estimate how the drying rate changes over the quasi-linear period from an initial rate of 0.0005 g h-1 to 0.0004 g h-1 – a 20% decrease in drying rate

## Slide 39: Dielectric loss or dielectric permittivity analysis?
Freeze drying of 5% sucrose (0.05μL)
Studied by Z-FDM
Notes: Now turning our attention to the impedance aspects of the Z–FDM measurement

## Slide 40: Drying: Image analysis vs Capacitance during drying of 0.05 µL 5%sucrose
I
II
III
IV
Linear relationship between real part capacitance C’ and pixel count (ice content) confirms the opportunity to use Z-FDM for drying rate estimation
A
B
I: Application of vacuum. Primary drying starts
II: Both gradients of imaginary and real part capacitance change towards the end of drying
II : end of primary drying
IV: Ramped to RT and capacitance remains unchanged with temperature
B
A
Notes: Again , we can look at the real and imaginary capacitances as measured at 1 point 6 kHz
To find that its the real part that gives a more reliable profile (click)
And so if we plot the real part against the pixel count
[click] we can see that there is good linear relationship
We might therefore conclude that Z-FDM could be used for a drying rate estimation

## Slide 41: Dielectric loss or dielectric permittivity analysis?
Annealing of 5% sucrose (0.05μL)
Studied by Z-FDM
Notes: Next we will take a look at how Z-FDM can be used to characterise the annealing stage

## Slide 42
Full process
A
B
C
D
E
Capacitance data measured at 1.6KHz
0.05 µL 5%sucrose
Annealing stages
Notes: Again we display the real and imaginary capacitances at 1 point 6 kHz above the temperature for the FDM stage
After the initial freezing stage
[click] there are three annealing cycles
[click] which bring the temperature up to – 25 deg C
which is above the glass transition of the sucrose solutions [click]

## Slide 43
Annealing (1.6KHz)
0.05 µL 5%sucrose
Structural changes on re-heating
decrease with each annealing
Excursions in temperature just above the glass transition
Sucrose Tg’
Notes: This slide provides a closer look at the impact of temperature-cycling on the Z-FDM response
But here, it is the imaginary capacitance that provides the most interest
[click]
you can see that excursions above the glass transition temperature result in inflections in the imaginary capacitance
[click]
However, what is more interesting is the change in the imaginary capacitance,
each time the temperature is increased through the glass transition
[click]
On first pass, the changes are so much larger, than subsequent annealing
Which suggest that the ice crystal structure is becoming more stable with each annealing

## Slide 44
Collapse of 5% sucrose (0.5 µL)
Studied by Z-FDM
Applications in primary drying : product collapse
Notes: In the last part we will take a look at how Z-FDM can be used for a more traditional application for freeze-drying microscopy, namely the study of the collapse temperature

## Slide 45: TASC – image analysis of sucrose solution
A
Adapted from: Ward, K. and Matejtschuk, P., 2019. Chapter 1 Characterization of Formulations for Freeze-Drying In: K. R. WARD and P. MATEJTSCHUK, eds, Lyophilization of Pharmaceuticals and Biologicals: New Technologies and Approaches. 1 edn. New York: Humana Press, pp. 1-33.
Reduces operator error in the analysis of the collapse temperature and can use for drying rate.
Tc −32.1°C
Tc(onset) −33.3˚C
Images coinciding with TASC features
onset of collapse at −33.3°C, and
full collapse occurring at −32.1°C
B
A
B
Collapsed layer
Notes: The first step was to use Biopharma’s TASC software for image analysis
Given that is less subjective than visual observations made by the operator
This allowed us to determine the onset of collapse at – 33.3 degrees C

## Slide 46: Collapse Observation at 1 kHz
Chart: log C'' (1kHz)
| 0 | 0.93300000000000005 | 1.883 | 2.8170000000000002 | 3.7669999999999999 | 4.7 | 5.65 | 6.5830000000000002 | 7.5330000000000004 | 8.4670000000000005 | 9.4169999999999998 | 10.367000000000001 | 11.3 | 12.25 | 13.183 | 14.132999999999999 | 15.067 | 16.016999999999999 | 16.95 | 17.899999999999999 | 18.850000000000001 | 19.783000000000001 | 20.733000000000001 | 21.667000000000002 | 22.617000000000001 | 23.55 | 24.5 | 25.433 | 26.382999999999999 | 27.317 | 28.266999999999999 | 29.216999999999999 | 30.15 | 31.1 | 32.033000000000001 | 32.982999999999997 | 33.917000000000002 | 34.866999999999997 | 35.799999999999997 | 36.75 | 37.683 | 38.633000000000003 | 39.582999999999998 | 40.517000000000003 | 41.466999999999999 | 42.4 | 43.35 | 44.283000000000001 | 45.232999999999997 | 46.167000000000002 | 47.116999999999997 | 48.067 | 49
 | 3.2576 | 3.27 | 3.288 | 3.2994 | 3.2838 | 1.4144 | 1.3381 | 1.4148 | 1.4767 | 1.4895 | 1.4885 | 1.4856 | 1.4977 | 1.4821 | 1.4987 | 1.4572 | 1.4264 | 1.4041 | 1.3929 | 1.3804 | 1.36 | 1.3386 | 1.342 | 1.3212 | 1.2951 | 1.2951 | 1.2561 | 1.2374 | 1.2517 | 1.2463 | 1.2194 | 1.2379 | 1.183 | 1.1819 | 1.19 | 1.1412 | 1.1392 | 1.1483 | 1.1551 | 1.1593 | 1.1401 | 1.1474 | 1.1672 | 1.1289 | 0.93112 | 0.5741 | 0.50616 | 0.28253 | 0.37474 | 0.55905 | 0.7266 | 0.66114 | 0.6565
Chart: Time (min)
Chart: log C' (1kHz)
| 0 | 0.93300000000000005 | 1.883 | 2.8170000000000002 | 3.7669999999999999 | 4.7 | 5.65 | 6.5830000000000002 | 7.5330000000000004 | 8.4670000000000005 | 9.4169999999999998 | 10.367000000000001 | 11.3 | 12.25 | 13.183 | 14.132999999999999 | 15.067 | 16.016999999999999 | 16.95 | 17.899999999999999 | 18.850000000000001 | 19.783000000000001 | 20.733000000000001 | 21.667000000000002 | 22.617000000000001 | 23.55 | 24.5 | 25.433 | 26.382999999999999 | 27.317 | 28.266999999999999 | 29.216999999999999 | 30.15 | 31.1 | 32.033000000000001 | 32.982999999999997 | 33.917000000000002 | 34.866999999999997 | 35.799999999999997 | 36.75 | 37.683 | 38.633000000000003 | 39.582999999999998 | 40.517000000000003 | 41.466999999999999 | 42.4 | 43.35 | 44.283000000000001 | 45.232999999999997 | 46.167000000000002 | 47.116999999999997 | 48.067 | 49
 | 3.5566 | 3.5137 | 3.4533 | 3.3614 | 3.2105 | 1.9672 | 1.9077 | 1.8695 | 1.8253 | 1.7814 | 1.7757 | 1.7803 | 1.7869 | 1.7787 | 1.7873 | 1.826 | 1.8557 | 1.8548 | 1.8522 | 1.8512 | 1.8492 | 1.8527 | 1.8463 | 1.8459 | 1.8436 | 1.8418 | 1.8324 | 1.8338 | 1.8306 | 1.8286 | 1.829 | 1.8251 | 1.8106 | 1.8089 | 1.8019 | 1.797 | 1.7817 | 1.7678 | 1.7648 | 1.7499 | 1.7295 | 1.707 | 1.684 | 1.6358 | 1.4778 | 1.3331 | 1.3152 | 1.2745 | 1.2876 | 1.2887 | 1.2934 | 1.2835 | 1.2715
Vacuum applied
I
I
III
III
II
II
NB: 0.5 μl of 5% Sucrose soluiton
Collapse temperature
determined at −34.5 °C

## Slide 47: Take home messages (from measurements at 1.6 KHz)
Real and imaginary part capacitances can be used for the determination of ice nucleation and ice growth rates
Pixel analysis works for drying rate determination
Real capacitance has a linear relationship with pixel count, and hence ice mass, so can be used for drying rate determination
Imaginary part capacitance can be used to study the annealing process but requires further work in order to be able to determine the glass transition temperature.
  Selection of a higher measurement frequency is likely to provide the answer to the glass transition temperature assessment
Step changes in drying rate (observed from real part capacitance) can be used to determine the collapse temperature

## Slide 48: Acknowledgements
for funding for Z-FDM development (FastLyo Project 133425)
In collaboration with ….
Anand Vadesa (PhD 2018-) Funded by UKRI – EPSRC
Evgeny Polygalov
TVIS technology development
Dr Yowwares Jeeraruangrattana
Thai Government Pharmaceutical Organization
Prof. Paul Dalby
Notes: In closing I’d like to thanks those made this work possible
[click] To Evgeny Polygalov, who designed and developed the original TVIS instrument
[click] To Dr Yowarres Jeeraruangrattana from the Thai Government Pharmaceutical Organization who’s PhD focussed on the development of applications for TVIS
[click] To Biopharma Process Systems (BPS) and Innovate UK for funding the Z-FDM development
[click] And to Anand Vadesa who is currently working on developing the Z-FDM applications on a PhD project
[click] funded by the EPSRC and co-supervised by Prof. Paul Dalby from UCL’s doctoral training college

## Slide 49: Thank you for listening

## Slide 50: Through Vial Impedance Spectroscopy (TVIS)
TVIS measurement relate to both the electrical resistance and electrical capacitance of the vial contents.
Chart: Log Frequency
| 1 | 1.0999912335446844 | 1.2000018654066018 | 1.3000082025538131 | 1.400002345927956 | 1.5000030680516931 | 1.6000030866277404 | 1.700002397142254 | 1.8000018278179688 | 1.9000009651534695 | 2 | 2.0999912335446846 | 2.2000018654066018 | 2.3000082025538129 | 2.4000023459279558 | 2.5000030680516931 | 2.6000249038929866 | 2.7000023971422538 | 2.8000362418279794 | 2.9000611027354806 | 3 | 3.1000257301078626 | 3.2001388538573807 | 3.3001605369513523 | 3.4001233554370809 | 3.5003188237463867 | 3.6003302305807652 | 3.7000543856282389 | 3.800655228145212 | 3.90049275542937 | 4 | 4.1009905230699646 | 4.200659016251719 | 4.3010299956639813 | 4.4006588497649739 | 4.5016890119157003 | 4.6020599913279625 | 4.7044336600521994 | 4.8027190075796815 | 4.9030899869919438 | 5 | 5.1106906972737542 | 5.204119982655925 | 5.3010299956639813 | 5.4259741609193757 | 5.5228744023138034
Time 0.3 h | 0.27396 | 0.24912 | 0.22663 | 0.2063 | 0.18797 | 0.17147 | 0.15668 | 0.14349 | 0.13183 | 0.12162 | 0.11284 | 0.10548 | 0.099574 | 0.095186 | 0.092431 | 0.091474 | 0.092551 | 0.095973 | 0.10215 | 0.11162 | 0.12501 | 0.14319 | 0.16715 | 0.198 | 0.23699 | 0.28544 | 0.34395 | 0.41214 | 0.48865 | 0.56683 | 0.63782 | 0.69048 | 0.71191 | 0.69725 | 0.65001 | 0.57934 | 0.49898 | 0.41726 | 0.34526 | 0.28116 | 0.22886 | 0.17991 | 0.14643 | 0.1181 | 0.089415 | 0.072054
Time 4 h | 0.099081 | 0.096153 | 0.095569 | 0.097591 | 0.10258 | 0.11101 | 0.12349 | 0.14075 | 0.16366 | 0.19315 | 0.23007 | 0.27492 | 0.32735 | 0.38533 | 0.44432 | 0.49685 | 0.53348 | 0.54588 | 0.53067 | 0.49125 | 0.43601 | 0.37424 | 0.31336 | 0.25794 | 0.20992 | 0.16948 | 0.13623 | 0.10926 | 0.087318 | 0.069838 | 0.055881 | 0.044566 | 0.035658 | 0.0285 | 0.02283 | 0.018246 | 0.014616 | 0.011669 | 0.0094101 | 0.0075633 | 0.0061328 | 0.0048349
Time 0.3 h | 0.26705 | 0.24478 | 0.21978 | 0.1979 | 0.17863 | 0.15615 | 0.14276 | 0.12639 | 0.11756 | 0.11024 | 0.10127 | 0.1004 | 0.098391 | 0.10089 | 0.10904 | 0.11009 | 0.11451 | 0.12496 | 0.13439 | 0.14683 | 0.16234 | 0.18119 | 0.20238 | 0.22944 | 0.26256 | 0.30331 | 0.35113 | 0.4089 | 0.47307 | 0.54005 | 0.60366 | 0.65431 | 0.67974 | 0.67269 | 0.63391 | 0.56955 | 0.49367 | 0.41413 | 0.34323 | 0.27998 | 0.22777
Time 4 h | 0.093429 | 0.092843 | 0.096342 | 0.10075 | 0.11232 | 0.12322 | 0.1435 | 0.1596 | 0.19684 | 0.23027 | 0.27214 | 0.31647 | 0.36246 | 0.41025 | 0.45421 | 0.48896 | 0.51147 | 0.51695 | 0.50285 | 0.46926 | 0.42098 | 0.36431 | 0.30625 | 0.25218 | 0.20511 | 0.16565 | 0.13355 | 0.10767 | 0.086605 | 0.069689 | 0.056026 | 0.045028 | 0.036377 | 0.029122 | 0.023205 | 0.018299 | 0.014688 | 0.011778 | 0.0095536 | 0.0077519 | 0.0063112
FPEAK
FPEAK
Liquid State
Solid State
Chart: Log Frequency
| 1 | 1.0999912335446844 | 1.2000018654066018 | 1.3000082025538131 | 1.400002345927956 | 1.5000030680516931 | 1.6000030866277404 | 1.700002397142254 | 1.8000018278179688 | 1.9000009651534695 | 2 | 2.0999912335446846 | 2.2000018654066018 | 2.3000082025538129 | 2.4000023459279558 | 2.5000030680516931 | 2.6000249038929866 | 2.7000023971422538 | 2.8000362418279794 | 2.9000611027354806 | 3 | 3.1000257301078626 | 3.2001388538573807 | 3.3001605369513523 | 3.4001233554370809 | 3.5003188237463867 | 3.6003302305807652 | 3.7000543856282389 | 3.800655228145212 | 3.90049275542937 | 4 | 4.1009905230699646 | 4.200659016251719 | 4.3010299956639813 | 4.4006588497649739 | 4.5016890119157003 | 4.6020599913279625 | 4.7044336600521994 | 4.8027190075796815 | 4.9030899869919438 | 5 | 5.1106906972737542 | 5.204119982655925 | 5.3010299956639813 | 5.4259741609193757 | 5.5228744023138034 | 5.6020599913279625 | 5.7569630370485534 | 5.8239109124113 | 5.9030899869919438 | 6
Time 13.1 h | 0.10929 | 0.1004 | 0.092502 | 0.087998 | 0.086049 | 0.088115 | 0.0938 | 0.10112 | 0.11429 | 0.13106 | 0.15364 | 0.18166 | 0.21583 | 0.25512 | 0.29985 | 0.34774 | 0.3951 | 0.43795 | 0.46981 | 0.48496 | 0.48002 | 0.45469 | 0.41262 | 0.36037 | 0.30465 | 0.25101 | 0.20331 | 0.16311 | 0.13007 | 0.10386 | 0.083113 | 0.06641 | 0.053298 | 0.042748 | 0.034381 | 0.027604 | 0.022219 | 0.017839 | 0.014449 | 0.011634 | 0.0093969 | 0.0073773 | 0.0059706 | 0.0046834 | 0.003604 | 0.003119 | 0.0043457 | 0.0022557 | 0.0032184 | 0.0030577 | 0.0023234
Time 16.1 h | 0.11007 | 0.10093 | 0.090991 | 0.082047 | 0.079543 | 0.078788 | 0.081723 | 0.087173 | 0.096992 | 0.11005 | 0.12829 | 0.15003 | 0.17689 | 0.20803 | 0.24102 | 0.27482 | 0.30518 | 0.32877 | 0.34107 | 0.33971 | 0.32434 | 0.2969 | 0.26113 | 0.22177 | 0.1829 | 0.1475 | 0.11733 | 0.092752 | 0.073068 | 0.057802 | 0.045912 | 0.036469 | 0.029123 | 0.02329 | 0.018706 | 0.015032 | 0.012128 | 0.0097734 | 0.0079623 | 0.0064562 | 0.0052363 | 0.0041244 | 0.0033647 | 0.0027806 | 0.0022635 | 0.0029162 | 0.0030408 | 0.0014411 | 0.0021872 | 0.0031647 | 0.0015537
Time 19.1 h | 0.096631 | 0.084665 | 0.074113 | 0.066591 | 0.062691 | 0.058864 | 0.058511 | 0.060476 | 0.065071 | 0.072096 | 0.081916 | 0.094578 | 0.10999 | 0.12716 | 0.1449 | 0.16219 | 0.17646 | 0.18582 | 0.1881 | 0.18242 | 0.16923 | 0.15032 | 0.12827 | 0.10587 | 0.085142 | 0.067241 | 0.052563 | 0.040958 | 0.031878 | 0.024951 | 0.019669 | 0.015531 | 0.012366 | 0.0098704 | 0.0079292 | 0.0063816 | 0.0051741 | 0.0042062 | 0.0034663 | 0.0028605 | 0.0023538 | 0.0018919 | 0.0016185 | 0.0014417 | 0.0019173 | 0.0019251 | 0.0021233 | 0.0015948 | 0.0015646 | 0.0023139 | 0.00072884
 | 0.11394 | 0.093481 | 0.077657 | 0.065696 | 0.057013 | 0.051186 | 0.047934 | 0.047103 | 0.048651 | 0.05264 | 0.059221 | 0.068608 | 0.08103 | 0.096621 | 0.11525 | 0.13624 | 0.15804 | 0.17801 | 0.19272 | 0.1989 | 0.19496 | 0.18175 | 0.16215 | 0.13967 | 0.1172 | 0.096485 | 0.078464 | 0.063316 | 0.050716 | 0.040549 | 0.032372 | 0.025721 | 0.020479 | 0.01627 | 0.012943 | 0.010261 | 0.008146 | 0.0064366 | 0.0051337 | 0.0040747 | 0.00326 | 0.0025268 | 0.0020378 | 0.0016303
 | 0.12912 | 0.10754 | 0.091277 | 0.079538 | 0.071764 | 0.067588 | 0.066822 | 0.06944 | 0.075575 | 0.085504 | 0.099635 | 0.11846 | 0.1425 | 0.17204 | 0.20691 | 0.24592 | 0.28627 | 0.32317 | 0.35038 | 0.36195 | 0.35498 | 0.33106 | 0.29542 | 0.25449 | 0.21357 | 0.17583 | 0.143 | 0.11539 | 0.092429 | 0.0739 | 0.058998 | 0.046874 | 0.037321 | 0.02965 | 0.023587 | 0.018699 | 0.014845 | 0.01173 | 0.0093551 | 0.0074254 | 0.0059407 | 0.0046044 | 0.0037133 | 0.0029707
 | 0.1177 | 0.10593 | 0.097045 | 0.090946 | 0.087643 | 0.087239 | 0.089948 | 0.096102 | 0.10617 | 0.12074 | 0.14056 | 0.16644 | 0.1992 | 0.2394 | 0.28694 | 0.3404 | 0.39622 | 0.44803 | 0.48732 | 0.50564 | 0.49835 | 0.46702 | 0.41851 | 0.36179 | 0.30443 | 0.25118 | 0.20462 | 0.16535 | 0.13261 | 0.10615 | 0.084841 | 0.067487 | 0.053798 | 0.042795 | 0.034092 | 0.027068 | 0.021523 | 0.017036 | 0.013612 | 0.010826 | 0.00868 | 0.0067451 | 0.0054527 | 0.0043739
increase
Drying time
Chart: Log Frequency
| 6 | 5.9030899869919438 | 5.8239109124113 | 5.7569630370485534 | 5.6020599913279625 | 5.5228744023138034 | 5.4259741609193757 | 5.3010299956639813 | 5.204119982655925 | 5.1106906972737542 | 5 | 4.9030899869919438 | 4.8027190075796815 | 4.7044336600521994 | 4.6020599913279625 | 4.5016890119157003 | 4.4006588497649739 | 4.3010299956639813 | 4.200659016251719 | 4.1009905230699646 | 4 | 3.90049275542937 | 3.800655228145212 | 3.7000543856282389 | 3.6003302305807652 | 3.5003188237463867 | 3.4001233554370809 | 3.3001605369513523 | 3.2001388538573807 | 3.1000257301078626 | 3 | 2.9000611027354806 | 2.8000362418279794 | 2.7000023971422538 | 2.6000249038929866 | 2.5000030680516931 | 2.4000023459279558 | 2.3000082025538129 | 2.2000018654066018 | 2.0999912335446846 | 2 | 1.9000009651534695 | 1.8000018278179688 | 1.700002397142254 | 1.6000030866277404 | 1.5000030680516931 | 1.400002345927956 | 1.3000082025538131 | 1.2000018654066018 | 1.0999912335446844 | 1
Time 4.4 h | 0.003361 | 0.0040465 | 0.0025946 | 0.0026214 | 0.0044553 | 0.0026323 | 0.0029087 | 0.0037366 | 0.0047149 | 0.0057564 | 0.0073092 | 0.0089323 | 0.011077 | 0.013703 | 0.017072 | 0.021236 | 0.026498 | 0.03301 | 0.041177 | 0.051293 | 0.064055 | 0.079683 | 0.099225 | 0.12384 | 0.15437 | 0.19231 | 0.23844 | 0.29224 | 0.35137 | 0.41125 | 0.46468 | 0.50437 | 0.52462 | 0.52356 | 0.50251 | 0.46708 | 0.42347 | 0.37253 | 0.32299 | 0.27537 | 0.23266 | 0.1978 | 0.16633 | 0.14424 | 0.12252 | 0.10889 | 0.097697 | 0.093226 | 0.09166 | 0.092155 | 0.093069
Time 4.5 h | 0.0034249 | 0.0041377 | 0.0027283 | 0.0027814 | 0.0046887 | 0.0029259 | 0.0032733 | 0.0042363 | 0.0053358 | 0.0065296 | 0.0082746 | 0.010141 | 0.012601 | 0.015587 | 0.01947 | 0.024233 | 0.030264 | 0.037737 | 0.047171 | 0.058901 | 0.073903 | 0.092482 | 0.11581 | 0.14538 | 0.18208 | 0.2274 | 0.28124 | 0.3416 | 0.40418 | 0.46243 | 0.50811 | 0.53414 | 0.53731 | 0.51809 | 0.48197 | 0.43577 | 0.38293 | 0.3311 | 0.28177 | 0.23748 | 0.20077 | 0.16802 | 0.14416 | 0.11848 | 0.11171 | 0.10187 | 0.09506 | 0.092791 | 0.094429 | 0.097904 | 0.10371
Time 4.6 h | 0.0036091 | 0.0043103 | 0.0029276 | 0.0030069 | 0.0049863 | 0.0032919 | 0.0037411 | 0.0048548 | 0.006126 | 0.0075084 | 0.0095269 | 0.011725 | 0.014579 | 0.018062 | 0.02259 | 0.028182 | 0.035264 | 0.044078 | 0.055262 | 0.069282 | 0.08729 | 0.10998 | 0.13862 | 0.17503 | 0.21981 | 0.27381 | 0.33549 | 0.40061 | 0.46249 | 0.51282 | 0.5432 | 0.54939 | 0.53148 | 0.49439 | 0.44517 | 0.39079 | 0.33577 | 0.28667 | 0.23998 | 0.20372 | 0.17181 | 0.14592 | 0.12721 | 0.11818 | 0.10489 | 0.098824 | 0.097908 | 0.099283 | 0.10394 | 0.11202 | 0.12205
Time 4.7 h | 0.0040254 | 0.0023197 | 0.0060162 | 0.0032852 | 0.0053707 | 0.003773 | 0.0043423 | 0.005672 | 0.0071637 | 0.0088006 | 0.011181 | 0.013771 | 0.017191 | 0.021329 | 0.026752 | 0.033478 | 0.04203 | 0.052722 | 0.066401 | 0.083738 | 0.10613 | 0.13436 | 0.17037 | 0.21573 | 0.27035 | 0.33347 | 0.40107 | 0.46603 | 0.51937 | 0.55253 | 0.55996 | 0.54171 | 0.50311 | 0.45097 | 0.39455 | 0.33876 | 0.28887 | 0.24104 | 0.20387 | 0.17339 | 0.14886 | 0.13225 | 0.11753 | 0.11 | 0.10482 | 0.10438 | 0.1074 | 0.1138 | 0.12408 | 0.13639 | 0.14993
Time 4.8 h | 0.0039527 | 0.0047899 | 0.0034912 | 0.0036734 | 0.0059298 | 0.004463 | 0.0052209 | 0.0068624 | 0.0086692 | 0.010687 | 0.013626 | 0.016821 | 0.021041 | 0.026213 | 0.03302 | 0.041432 | 0.052261 | 0.065911 | 0.083539 | 0.10606 | 0.13545 | 0.17252 | 0.21928 | 0.27665 | 0.34237 | 0.41271 | 0.47977 | 0.53353 | 0.56486 | 0.56874 | 0.5461 | 0.50317 | 0.44813 | 0.38872 | 0.33224 | 0.28045 | 0.23905 | 0.20172 | 0.17254 | 0.14998 | 0.13098 | 0.12232 | 0.11386 | 0.11155 | 0.11412 | 0.11812 | 0.12658 | 0.13848 | 0.15361 | 0.17099 | 0.18866
Time 4.9 h | 0.0043188 | 0.0052277 | 0.0039868 | 0.0042288 | 0.0066529 | 0.0053479 | 0.0063485 | 0.0083796 | 0.010604 | 0.013107 | 0.016765 | 0.020805 | 0.02609 | 0.032614 | 0.041224 | 0.052023 | 0.065957 | 0.083695 | 0.10683 | 0.13651 | 0.17523 | 0.22353 | 0.28261 | 0.35128 | 0.42376 | 0.49222 | 0.54583 | 0.5749 | 0.57491 | 0.54814 | 0.50162 | 0.4443 | 0.38384 | 0.32634 | 0.27564 | 0.23272 | 0.19908 | 0.1717 | 0.1495 | 0.13558 | 0.12502 | 0.11938 | 0.11838 | 0.12437 | 0.13062 | 0.13992 | 0.15492 | 0.1723 | 0.19073 | 0.21306 | 0.23377
Time 5 h | 0.0049133 | 0.0058042 | 0.0046338 | 0.0049712 | 0.0076664 | 0.0066031 | 0.0079479 | 0.010533 | 0.013358 | 0.01657 | 0.021298 | 0.026516 | 0.033397 | 0.041936 | 0.053268 | 0.067599 | 0.086277 | 0.11024 | 0.14161 | 0.18183 | 0.2334 | 0.29549 | 0.36662 | 0.44167 | 0.50969 | 0.5605 | 0.58424 | 0.57776 | 0.54458 | 0.49349 | 0.43374 | 0.3731 | 0.31662 | 0.26729 | 0.22557 | 0.19336 | 0.16657 | 0.14984 | 0.13717 | 0.1291 | 0.12498 | 0.12759 | 0.13258 | 0.1444 | 0.15601 | 0.17194 | 0.19151 | 0.21398 | 0.23437 | 0.26066 | 0.28203
Time 5.1 h | 0.0051615 | 0.0065394 | 0.0054847 | 0.0059393 | 0.0090001 | 0.0082333 | 0.010001 | 0.013324 | 0.016914 | 0.021051 | 0.027147 | 0.03396 | 0.042946 | 0.054219 | 0.069319 | 0.088593 | 0.11394 | 0.14657 | 0.18909 | 0.24251 | 0.30812 | 0.38167 | 0.45767 | 0.52576 | 0.57299 | 0.59132 | 0.57824 | 0.5397 | 0.48481 | 0.42344 | 0.36292 | 0.3071 | 0.25963 | 0.22024 | 0.18846 | 0.16573 | 0.14947 | 0.13846 | 0.13032 | 0.13113 | 0.1334 | 0.1422 | 0.15348 | 0.16641 | 0.18887 | 0.2096 | 0.23238 | 0.25699 | 0.28353 | 0.3063 | 0.32649
-38 oC
-18 oC
Monitoring Phase Behaviour (ice nucleation temperature and solidification end points
FPEAK temperature calibration for predicting temperature of the product in primary drying
Drying rate surrogate (from dC″PEAK /dt )
  C′ (real part of the complex capacitance) is highly sensitive to low ice volumes; therefore it could be used for determination end point of primary drying
Notes: Eg temperature cycling below to calibrate Fpeak for temperature (in order to predict product temperatures in primary drying) and the compensate cpeak for temperature so that it can used to monitor ice content and hence drying rate
Eg 2 left graph: monitoring phase behaviour (ice nucleation temperatures and solidufication end points)

## Slide 51: Temperature Calibration
Chart: Log Frequency
| 6 | 5.9030899869919438 | 5.8239109124113 | 5.7569630370485534 | 5.6020599913279625 | 5.5228744023138034 | 5.4259741609193757 | 5.3010299956639813 | 5.204119982655925 | 5.1106906972737542 | 5 | 4.9030899869919438 | 4.8027190075796815 | 4.7044336600521994 | 4.6020599913279625 | 4.5016890119157003 | 4.4006588497649739 | 4.3010299956639813 | 4.200659016251719 | 4.1009905230699646 | 4 | 3.90049275542937 | 3.800655228145212 | 3.7000543856282389 | 3.6003302305807652 | 3.5003188237463867 | 3.4001233554370809 | 3.3001605369513523 | 3.2001388538573807 | 3.1000257301078626 | 3 | 2.9000611027354806 | 2.8000362418279794 | 2.7000023971422538 | 2.6000249038929866 | 2.5000030680516931 | 2.4000023459279558 | 2.3000082025538129 | 2.2000018654066018 | 2.0999912335446846 | 2 | 1.9000009651534695 | 1.8000018278179688 | 1.700002397142254 | 1.6000030866277404 | 1.5000030680516931 | 1.400002345927956 | 1.3000082025538131 | 1.2000018654066018 | 1.0999912335446844 | 1
Time 6.5 h | -0.012915 | -0.012903 | -0.026573 | -0.022527 | -0.0057054 | -0.0026676 | -0.00087407 | 0.0039471 | 0.0095664 | 0.013418 | 0.018179 | 0.022836 | 0.028519 | 0.035311 | 0.043802 | 0.053906 | 0.066287 | 0.081042 | 0.098685 | 0.1197 | 0.14499 | 0.17447 | 0.20948 | 0.25138 | 0.30065 | 0.35896 | 0.42715 | 0.50407 | 0.58707 | 0.67087 | 0.74622 | 0.80354 | 0.83309 | 0.82941 | 0.79582 | 0.73855 | 0.66701 | 0.58987 | 0.51096 | 0.43831 | 0.37211 | 0.31726 | 0.27059 | 0.23268 | 0.20255 | 0.18131 | 0.16669 | 0.15777 | 0.15468 | 0.15673 | 0.16341
Time 6.6 h | -0.012604 | -0.013685 | -0.026927 | -0.022578 | -0.0051854 | -0.0021223 | 0.00010962 | 0.0053562 | 0.011295 | 0.01547 | 0.020676 | 0.025906 | 0.03232 | 0.039977 | 0.049615 | 0.061147 | 0.07522 | 0.091989 | 0.1123 | 0.13642 | 0.16572 | 0.20021 | 0.24161 | 0.29132 | 0.34982 | 0.4183 | 0.49637 | 0.581 | 0.66699 | 0.74648 | 0.80813 | 0.84325 | 0.84529 | 0.81459 | 0.75758 | 0.6857 | 0.6058 | 0.52528 | 0.44909 | 0.38302 | 0.32208 | 0.2765 | 0.2361 | 0.20787 | 0.18311 | 0.1676 | 0.15803 | 0.15449 | 0.1559 | 0.16178 | 0.17175
Time 6.7 h | -0.012524 | -0.013922 | -0.027192 | -0.022092 | -0.0042742 | -0.0010028 | 0.0016359 | 0.0072245 | 0.013496 | 0.018129 | 0.02406 | 0.030067 | 0.037557 | 0.046412 | 0.057674 | 0.071133 | 0.087638 | 0.10737 | 0.1314 | 0.16011 | 0.19527 | 0.23687 | 0.28704 | 0.34713 | 0.41679 | 0.49639 | 0.58331 | 0.6719 | 0.75364 | 0.81829 | 0.85529 | 0.85913 | 0.82927 | 0.77209 | 0.69594 | 0.61445 | 0.53185 | 0.45545 | 0.38652 | 0.32785 | 0.27696 | 0.23823 | 0.20743 | 0.18577 | 0.16844 | 0.1597 | 0.15545 | 0.15679 | 0.16238 | 0.17215 | 0.18526
Time 6.8 h | -0.011996 | -0.011808 | -0.024771 | -0.020627 | -0.0030166 | 0.000587 | 0.0033338 | 0.0093432 | 0.016102 | 0.021508 | 0.028552 | 0.035744 | 0.044642 | 0.055278 | 0.068773 | 0.084933 | 0.10491 | 0.12878 | 0.15805 | 0.19327 | 0.23651 | 0.28778 | 0.34911 | 0.42154 | 0.5032 | 0.59242 | 0.68359 | 0.76744 | 0.83248 | 0.86927 | 0.87098 | 0.83871 | 0.77865 | 0.70125 | 0.61521 | 0.53287 | 0.45455 | 0.38692 | 0.32646 | 0.278 | 0.23763 | 0.2086 | 0.18548 | 0.17312 | 0.16153 | 0.15785 | 0.15959 | 0.16567 | 0.17553 | 0.18843 | 0.20444
Time 6.9 h | -0.011319 | -0.011167 | -0.023955 | -0.019624 | -0.0014742 | 0.0024193 | 0.0057065 | 0.01263 | 0.020163 | 0.026517 | 0.034957 | 0.04367 | 0.054571 | 0.067657 | 0.084297 | 0.10431 | 0.12912 | 0.15891 | 0.19551 | 0.23964 | 0.29363 | 0.3571 | 0.43154 | 0.51685 | 0.60849 | 0.70173 | 0.78638 | 0.85051 | 0.88321 | 0.87986 | 0.84212 | 0.77794 | 0.69646 | 0.61108 | 0.52514 | 0.44886 | 0.37896 | 0.32372 | 0.27635 | 0.23844 | 0.20681 | 0.18754 | 0.17249 | 0.16568 | 0.16236 | 0.16473 | 0.17107 | 0.18117 | 0.19503 | 0.20989 | 0.2274
Time 7 h | -0.010092 | -0.0099327 | -0.02249 | -0.017968 | 0.00075188 | 0.005072 | 0.0090852 | 0.017175 | 0.025806 | 0.033487 | 0.043827 | 0.054728 | 0.068414 | 0.084873 | 0.10592 | 0.13132 | 0.16278 | 0.20072 | 0.24723 | 0.30288 | 0.37011 | 0.44735 | 0.53502 | 0.63012 | 0.7245 | 0.80853 | 0.86931 | 0.89645 | 0.88498 | 0.84006 | 0.76986 | 0.68693 | 0.59985 | 0.51541 | 0.43793 | 0.3732 | 0.31754 | 0.27284 | 0.23606 | 0.20955 | 0.18919 | 0.17734 | 0.17035 | 0.17042 | 0.17204 | 0.17937 | 0.19 | 0.203 | 0.21806 | 0.23451 | 0.25168
Time 7.1 h | -0.008876 | -0.0084316 | -0.020757 | -0.015909 | 0.003746 | 0.0086648 | 0.013614 | 0.023234 | 0.033378 | 0.042791 | 0.055836 | 0.0697 | 0.087185 | 0.10829 | 0.13531 | 0.16794 | 0.20831 | 0.2568 | 0.31563 | 0.38496 | 0.46665 | 0.55703 | 0.65373 | 0.74935 | 0.83107 | 0.88672 | 0.90617 | 0.88613 | 0.83269 | 0.7578 | 0.67124 | 0.58439 | 0.50268 | 0.42817 | 0.36427 | 0.31235 | 0.27016 | 0.23733 | 0.21354 | 0.19248 | 0.18413 | 0.17819 | 0.1773 | 0.17861 | 0.1889 | 0.20021 | 0.20958 | 0.22843 | 0.24153 | 0.25824 | 0.27417
Time 7.2 h | -0.0071135 | -0.006478 | -0.018163 | -0.012987 | 0.0077611 | 0.013521 | 0.019676 | 0.031269 | 0.043471 | 0.055271 | 0.071942 | 0.089792 | 0.11234 | 0.1396 | 0.17447 | 0.21651 | 0.26809 | 0.3293 | 0.40224 | 0.4859 | 0.58036 | 0.67849 | 0.77309 | 0.85199 | 0.90134 | 0.91205 | 0.88342 | 0.82276 | 0.74205 | 0.65417 | 0.56724 | 0.48782 | 0.41671 | 0.35611 | 0.30573 | 0.26661 | 0.23475 | 0.21377 | 0.19892 | 0.18772 | 0.18072 | 0.18576 | 0.19075 | 0.20396 | 0.21078 | 0.22434 | 0.23723 | 0.25253 | 0.26698 | 0.27987 | 0.29411
FPEAK profile during annealing has ‘similar’ profile with product temperature.
Assuming thermal equivalence between the thermocouple (TC) vial and TVIS vial, then the temperature calibration from annealing might be employed for the prediction of temperature during primary drying
-40 oC
Chart: Time / h
-20 oC
Chart: Log FPEAK
| 2.7147290000000002 | 2.740151 | 2.7674099999999999 | 2.7947799999999998 | 2.8238530000000002 | 2.8529260000000001 | 2.881999 | 2.913297 | 2.9466929999999998 | 2.9797709999999999 | 3.0148079999999999 | 3.051647 | 3.0886429999999998 | 3.1257830000000002 | 3.1645470000000002 | 3.2033109999999998 | 3.2443939999999998 | 3.2852670000000002 | 3.325952 | 3.3664649999999998 | 3.409141 | 3.4500139999999999 | 3.4906990000000002 | 3.531212 | 3.5715690000000002 | 3.6126520000000002 | 3.6512180000000001
Re-heating | -41.6 | -40.5 | -39.9 | -38.8 | -38.2 | -37.2 | -36.3 | -35.3 | -34.4 | -33.5 | -32.5 | -31.6 | -30.6 | -29.4 | -28.3 | -27.5 | -26.3 | -25.4 | -24.3 | -23.4 | -22.2 | -21.4 | -20.5 | -19.4 | -18.5 | -17.3 | -16.5
Shelf Temp.
Product Temp.
TVIS
Temperature
FPEAK
Notes: Full Shelf Water Study_180817_Ch1 (Fill factor 0.7) 3mm gap –Dual electrode
Re-heat
Time/hr. TC1
6.5 -39.9
6.6 -37.2
6.7 -34.4
6.8 -31.6
6.9 -28.3
7.0 -25.4
7.1 -22.2
7.2 -19.4

## Slide 52: Temperature Prediction in Primary Drying
Good agreement between product temperature (by TC) and T(FPEAK)
Chart: Time / h
Temperature calibration curve selected for temperature prediction in primary drying : T(FPEAK)
Chart: Log FPEAK
| 2.7147290000000002 | 2.740151 | 2.7674099999999999 | 2.7947799999999998 | 2.8238530000000002 | 2.8529260000000001 | 2.881999 | 2.913297 | 2.9466929999999998 | 2.9797709999999999 | 3.0148079999999999 | 3.051647 | 3.0886429999999998 | 3.1257830000000002 | 3.1645470000000002 | 3.2033109999999998 | 3.2443939999999998 | 3.2852670000000002 | 3.325952 | 3.3664649999999998 | 3.409141 | 3.4500139999999999 | 3.4906990000000002 | 3.531212 | 3.5715690000000002 | 3.6126520000000002 | 3.6512180000000001
Re-heating | -41.6 | -40.5 | -39.9 | -38.8 | -38.2 | -37.2 | -36.3 | -35.3 | -34.4 | -33.5 | -32.5 | -31.6 | -30.6 | -29.4 | -28.3 | -27.5 | -26.3 | -25.4 | -24.3 | -23.4 | -22.2 | -21.4 | -20.5 | -19.4 | -18.5 | -17.3 | -16.5
Shelf Temperature (
Before
drying
during drying
TC
T(FPEAK)
Before drying
TC
T(FPEAK)
during drying
>
Notes: Full Shelf Water Study_281016_Ch1 (Fill factor 0.9) 3mm gap

## Slide 53: Compensation of C″PEAK by T(FPEAK)
Chart: Temperature /oC
| -41.6 | -40.5 | -39.9 | -38.799999999999997 | -38.200000000000003 | -37.200000000000003 | -36.299999999999997 | -35.299999999999997 | -34.4 | -33.5 | -32.5 | -31.6 | -30.6 | -29.4 | -28.3 | -27.5 | -26.3 | -25.4
Re-heating | 0.8231 | 0.82683 | 0.83065 | 0.83454 | 0.83854 | 0.84264 | 0.84676 | 0.85083 | 0.85491 | 0.85875 | 0.86246 | 0.86594 | 0.86931 | 0.87262 | 0.87576 | 0.87873 | 0.88151 | 0.88413
Chart: Time / h
Ĉ″PEAK
C″PEAK
13.67 h
Chart: Time / h
13.67 h drying
starts
Thermocouple
T(FPEAK)
195 µbar
Chart: Temperature / oC
| -30 | -31 | -32 | -33 | -34 | -35 | -36 | -37 | -38 | -39 | -40 | -41 | -42 | -43 | -44 | -45
 | 0.37 | 0.34 | 0.31 | 0.28 | 0.25 | 0.22 | 0.2 | 0.18 | 0.16 | 0.14 | 0.12 | 0.11 | 0.1 | 0.09 | 0.08 | 0.07
195 µbar
−36 oC
T(FPEAK) during primary drying is used for compensation

## Slide 54: Drying rate calculation
Chart: Time / h
Drying rate (g/h) for Ĉ″PEAK
(0.83 pF, 14.3 h)
(0.47 pF, 17.4 h)

## Slide 55: Summary
Temperature calibration of the TVIS parameter () for ice during an additional temperature cycling stage applied to a prediction of ice temperatures during the initial (few hours) of primary drying
Temperature compensation of TVIS parameter () allows for an accurate estimation of ice mass during primary drying as evidenced by comparable results of drying rate between the determined by TVIS and that determined (gravimetrically) by loss weight
Non-invasive real time information for characterising the freeze drying process

## Slide 56: Future Work
Development mapping a drying characteristics from lab scale to production
  Determination of heat transfer coefficients ()
  Determination of dry layer resistance () to predict drying efficiency
Investigation the molecular dynamic of the unfrozen fraction
  Monitoring product stability
  Examine the mechanical strength of the freeze dried product (i.e. collapse behaviour)
Develop (new) continuous drying technologies

## Slide 57: Further Reading
Introduction to TVIS theory
Description of the measurement principles
Dielectric loss and relaxations mechanisms (liquid and frozen states)

## Slide 58: Further Reading
Chapter 5 Through Vial Impedance Spectroscopy (TVIS) A New Method for Determining the Ice Nucleation Temperature and the Solidification End point
Notes: Baook cover

## Slide 60: Glass Transition (Tgʹ) Determination
Chart: 1000/T (K)
| 4.4296788482835003 | 4.4120891242003104 | 4.3907793633369865 | 4.3734966105401334 | 4.3506634761801184 | 4.3318171973142814 | 4.3094160741219545 | 4.2872454448017194 | 4.2653017701002351 | 4.2417815482502652 | 4.220299641274539 | 4.1990342221288985 | 4.1744938426215805 | 4.1536863966770445 | 4.1296716911005582 | 4.1093075816724891 | 4.0858018386108279 | 4.0625634775543373 | 4.0395879620278725 | 4.0201005025125625 | 3.9992001599680025 | 3.9785160135269551 | 3.9596119580281135 | 3.9408866995073897 | 3.9192631785224381 | 3.9070130884938465 | 3.8933229511387974 | 3.8842493688094781 | 3.8767202946307391 | 3.8707180181923788 | 3.8647342995169121
Unfrozen fraction | 22.0313 | 21.981 | 21.9288 | 21.8645 | 21.806 | 21.751 | 21.6777 | 21.5918 | 21.5013 | 21.4036 | 21.2996 | 21.189 | 21.0727 | 20.9525 | 20.8199 | 20.6769 | 20.517 | 20.3563 | 20.1867 | 20.0058 | 19.804 | 19.583 | 19.3351 | 19.0636 | 18.7557 | 18.4618 | 18.2039 | 17.9839 | 17.8034 | 17.6461 | 17.5186
ln R1B | 22.0313 | 21.981 | 21.9288 | 21.8645 | 21.806 | 21.751 | 21.6777 | 21.5918 | 21.5013 | 21.4036 | 21.2996 | 21.189 | 21.0727 | 20.9525 | 20.8199 | 20.6769 | 20.517 | 20.3563 | 20.1867 | 20.0058 | 19.804 | 19.583 | 19.3351 | 19.0636 | 18.7557 | 18.4618 | 18.2039 | 17.9839 | 17.8034 | 17.6461 | 17.5186
ln R1B | 22.0313 | 21.981 | 21.9288 | 21.8645 | 21.806 | 21.751 | 21.6777 | 21.5918 | 21.5013 | 21.4036 | 21.2996 | 21.189 | 21.0727 | 20.9525 | 20.8199 | 20.6769 | 20.517
R1A
C1A
R1B
C1B
C2
Linear scale
Log scale
5.83 h
6.33 h
Initial (5.33 h)
5% w/v Lactose solution
Below Tgʹ the changes in product resistance follows Arrhenius
Above Tgʹ VTF function models the resistance profile.
-9.99 -16.74 -23.15 -29.25 -35.05 -40.59 -45.88 -50.93 oC
Notes: Full shelf 5%w/v Lactose in ultrapure water 25Nov16_CH4

## Slide 61: Lactose Dried Product Resistance (RP)
Chart: Temp. /oC
Chart: Pressure / torr
9.1 mm
3 mm
Chart: Time/h
Chart: Dry Layer Thickness (cm)
1.75cm2·Torr·h·g-1
Notes: Version 14
If we are now calculating Rp then we only need to show the product temperature (Tfpeak) and the condenser temperature
Then below that the values for partial pressure – to replace the log Fpeak plot
Then the drying rate (ice vs time) and not c”peak vs time on the bottom left
Replace the top right with my new Rp values
Full shelf 5%w/v Lactose in ultrapure water 23Jan17-CH3 (Fill factor 0.7 = 3.04 g)-3mm above base electrode
From the literature (Pikal (1985) PDA Journal of Pharmaceutical Science and Technology, 39(3), pp.115-139.): Rs ~0.33 Torr·h·g-1.
The temperatures we are using (calculated from log Fpeak) have not been smoothed and the values for C"peak (although taken from the moving average) both have scatter to them - hence why the plot of Rp vs dry layer is quite noisy
Rp starts at 2 (which I presume is the stopper resistance) then it increases as the dry layer develops in thickness up to 3 mm - which is the point at which micro-collapse has happened. At that point, the overall resistance decreases which means that microcollapse has also occurred in the layer above the ice - which already has no ice. If there was no microcollapse in that layer then Rp would stay constant after 3 mm of the dry layer develops. Instead, Rp drops to a new value at ~ 4mm dry layer (when microcollapse occurs) and doesn't change after that. I presume that is because a more dramatic microcollapse occurs in the layers that develop below 4 mm - which are seen on our SEM as large pores and so the layers below the top 3 mm do not have a measureable dry layer resistance.
Milton et al. study product resistance by comparing the direct vial method and MTM (data shown in literature are from direct vial technique according to Pikal's method). They concluded that the product resistance value from MTM agree with direct vial technique and has the same pattern. For lactose, they reported that product resistance increases continuously with thickness up to the onset of collapse (below about -30 Celcius).

## Slide 62: Lactose Dried Product Resistance (RP)
Middle layer
Micro-collapse
Top layer
Fine pores
Bottom layer
Full collapse
500X
3 mm
500X
500X
Chart: Dry Layer Thickness (cm)
3 mm
Notes: Full shelf 5%w/v Lactose in ultrapure water 23Jan17-CH3 (Fill factor 0.7 = 3.04 g)-3mm above base electrode
Img: 5%lactose_16Nov16-Ng03-10a

## Slide 63: Examples of Biopharmaceuticals Therapy
Cardiovascular system
Factor VIII helps blood to clot
Treatment hemophilia
Growth hormone
Endocrine system
Integumentary system
Nivolumab
Treatment Melanoma

## Slide 64: Monoclonal antibodies (mAb)
mAbs used for treatment cancer
Notes: Glassman PM, Balthasar JP. Mechanistic considerations for the use of monoclonal antibodies for cancer therapy. Cancer Biology & Medicine. 2014;11(1):20-33. doi:10.7497/j.issn.2095-3941.2014.01.002.

## Slide 65: Interdigitated electrodes
Interdigitated electrodes have been used in past for the prediction of lyophile collapse temperature
Mackenzie, A. P., Evans, S. A. and Morris,. Prediction of Lyophile Collapse Temperature by Dielectric Analysis Prediction of Lyophile Collapse Temperature by Dielectric Analysis, PDA J Pharm Sci and Tech 1994, 48 318-329.
A: Showing individual components of a single surface, co-planer, interdigitated-comb sensor and B: the complete sensor
A
B
Notes: MORRIS, K.R. et al. Prediction of Lyophile Collapse Temperature by Dielectric Analysis Prediction of Lyophile Collapse Temperature by Dielectric Analysis, PDA J Pharm Sci and Tech 1994, 48 318-329.
Evans, S.A. et al. Dielectric Characterization of Thermodynamic First Order Events in Model Frozen Systems Intended for Lyophilization Dielectric Characterization of Thermodynamic First Order Events in Mode ! Frozen Systems Intended for Lyophiiization, PDA J Pharm Sci and Tech 1995, 49 2-8

## Slide 66: Example interdigitated electrode (gold on glass)
Commercial IDE – MicruxTM
10 m
10 m
Electrode gap
Electrode width
Light aperture 1.3mm diameter
Width of the electrode 3.5 mm Ø
Notes: http://www.linkam.co.uk/fdcs196-specifications
https://static1.squarespace.com/static/556d800ae4b0e8f91507450c/t/56cf3686f8baf3fe56cc48e2/1456420522066/FDCS196_T95_manual.pdf

## Slide 67: Design of IDE holder
IDE dimensions:
10 x 6 x 0.75 mm
10mm
Top view
6 mm
16mm
6 mm
10 mm
0.85 mm*
* different height of IDE adaptors used for initial assessment:
0.85 mm
0.90 mm
0.95 mm
1.00 mm
*IDE height 0.75 mm
*
IDE is lower than the adapter and sample height derived between difference between then IDE adaptor size
Theoretical sample height
Notes: https://static1.squarespace.com/static/556d800ae4b0e8f91507450c/t/56cf3686f8baf3fe56cc48e2/1456420522066/FDCS196_T95_manual.pdf